## Slide 1: ATLAS07 evaluation in Japan
<number>
Univ. Tsukuba
(K. Hara, M. Hatano, S. Mitsui, M.Yamada)
KEK
(T. Kohriki, S. Terada, Y. Ikegami, Y. Unno)
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 2: ATLAS07
<number>
PreSeries I (delivery1) :
P10 (stop=10x1012/cm2), P8r2 (stop+spray=8+2 1012)
irradiated with 70-MeV protons in March 2008
with reactor neutron in April 2008
with 60Co in Sept 2008
PreSereis II (delivery2) : P2, P4, r2, P2r2
irradiated with protons in Nov. 2008.
PreSeries II (delivery3) : P2, P4, r2, r4, P8r2
proton irradiation scheduled in 2-4 March
few typical samples irradiated with 60Co in Feb. 2009
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 3: Strip Isolation – proton irradiation –
<number>
Delivery 1
Isolation voltage: bias voltage where DC-DC resistance reaches the asymptotic value within 10%
Delivery 2
Pstop of (2-4)x1012/cm2 is substantially weaker than ~ 10x1012/cm2
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 4: Strip Isolation – during 60C –
<number>
Delivery 3
0:P4z2 1:P4z3
2:P4z4A 3:P4z4B 4:P4z4C 5:P4z4D
Bias = 300V during irradiation @0.1 kGy/h
All behaved similarly – “isolation” point reached 300 V in a few hrs and stayed constant for 4 days we tested.
Curves measured right after the source is removed are distorted: E-field may be adjusted to achieve isolation at 300V with source on…
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 5: Strip Isolation – during 60C –
<number>
Delivery 3
0:P4z2 1:P4z3
2:P4z4A 3:P4z4B 4:P4z4C 5:P4z4D
Bias = 300V during irradiation @0.1 kGy/h
Delivery 1
12:P8r2_z3 13:P10_z3
14:P10_z4A 15:P8r2_z4
Four samples irradiated 5 months ago
Similar behavior to the newly irradiated samples
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 6: PTP - delivery3 non-irrad -
<number>
P8r2
P2
PT voltage: Design A < others
depends on isolation structure
( two extrems)
*Eff. R = (induced I)/(V applied to DC wrt BR)
Bias=300V, T= -20degC
PT voltage is higher for “tighter” isolation
P8r2 > r4 > P4 > r2 >P2
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 7: PTP after proton irradiation
<number>
*Eff. R = (induced I)/(V applied to DC wrt BR)
delivery2
Proton 13x1014
non-irrad VPT larger than delivery 3
Small structure dependence …
Non irrad
Post-irrad: P2r2 ~ P4 > r2 > P2
(all values are ~comfortable)
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 8: PTP after slight irradiation
<number>
Proton 13x1014
delivery3
Non irrad
VPT decreases initially
(then increases to asymptotic value ~30V)
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 9: IV history of a sample under 60Co
<number>
W44Z3P9 (spray 4x1012/cm2)
received 110 Gy before
this series of measurement
additional 390 Gy accumulated
bias kept at 150V during irradiation
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 10: Collected charge, evaluated with Sr 
<number>
n: Delivery 1 p: Delivery 2
FDVs for neutrons seem larger
more charge collectable for n at higher bias
Sum charge of two strips at
center with cut applied to
their neighbors
General tendency is consistent with laser results
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 11: Full Depletion Voltage
<number>
Proton and neutron damages (annealing behavior) may be different.
Or, different irradiation conditions (temperature, biasing during irradiation, …)
ex: for 1015/cm2 irradiation, irradiation time is 9 min (n) vs. 90 min (p)
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 12: Summary
<number>
ATLAS07 is being evaluated through proton/neutron/ irradiation
I-V : damage constant is consistent with n-bulk sensors (not covered)
MD voltage found to decrease initially in ~1kGy radiation.
ISO : Pstop of 1013/cm2 is better than a fewx1012/cm2
Pspray of 4x1012/cm2 is too dense (not covered)
Isolation (or DC-DC resistance) is found to change at 100Gy/h irradiation,
with isolation voltage approaching the bias voltage.
The time scale & stability is dependent on the isolation structure.
PTP : PT voltage before irradiation 15-60V, dependent on isolation structure.
PT voltage after irradiation is 40-50V with small structure dependence.
Rbias & Cint: small degradation by irradiation (not covered)
CCE : evaluated using 90Sr and infrared laser.
CCE(Vb=500V)~40%(60%) for n(p) of 1015/cm2
Full Depletion : evaluated using 90Sr and infrared laser and with C-V
The VFD evolution is consistently quicker for neutron damage.
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 13: Backup
<number>
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 14: Punch Through Protection Design
<number>
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 15: Samples – delivery 2 -
<number>
P2r2 : p-stop 2×1012 + p-spray 2×1012 /cm2
P2 : p-stop 2×1012 /cm2
P4 : p-stop 4×1012 /cm2
r2 : p-spray 2×1012 /cm2
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 16: IV : P-spray concentration
<number>
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 17: PTP Delivery 3
<number>
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>

## Slide 18: Rbias & Cint
<number>
K. Hara (U. Tsukuba) 2/23/2009 ATLAS Upgrade Week
Notes: <number>