## Slide 1: ATLAS07 Bulk Property
K. Hara (U. Tsukuba)‏
summarizing the data from
Tsukuba/KEK, Liverpool, UCSC on
I-V, C-V, FDV of pre- and post-irradiated mini SSDs
ATLAS Tracker Upgrade Workshop
NIKHFF 2008 Nov 5

## Slide 2: I-V pre-irradiation
Z4
Z3
Z1
Z5
<I>@220V=7.5nA (25oC)‏
Leakage current as low as of n-bulk FZ
typical HPK n-bulk microstrip
~ 4 nA/cm2
PreSeries-I samples irradiated by Tsukuba/KEK

## Slide 3: Irradiation
70 MeV protons at CYRIC, Tohoku U.
a few 10 min ~ a few hr, to (2, 6, 13) x1014 1-MeV neq/cm2
NIEL factor (p/1-MeV n) = 1.3
-10oC and biased at 100 V
Reactor neutrons at JSI, Ljubljana
at 1.9 x1012 n/cm2/sec, to (2, 5, 10) x1014 1-MeV neq/cm2
NIEL factor (<n>/1-MeV n) = 0.88
no bias and at room temperature
800 MeV protons at Los Alamos NL
stopped at (0.15) x1014 p/cm2 after operator fault: TID=5 kGy
NIEL factor (p/1-MeV n) = ~1
no bias and at room temperature
Tsukuba/KEK-Liverpool
Tsukuba/KEK-Liverpool
UCSC

## Slide 4: Bulk Annealing
Tsukuba/KEK
ATLAS06
FZ_pure (ATLAS06) and FZ (ATLAS07) are from the same batch.
Irradiated Tsukuba/KEK data in the following pages are after 80min annealing
Annealing in CCE is presented in different talk
Irradiated with 70 MeV protons to 2x1014
Tsukuba/KEK
with neutrons to 2x1014
annealing in FDV evaluated from C-V and laser CC-V curves

## Slide 5: I-V irradiated after annealing
p13.2,n10.0 (x1014)‏
p6.0,n5.0
p2.1,n2.0
Pstop only
Pstop+Pspray
proton z1
proton z3
proton z4
neutron z3
neutron z5
Tsukuba/KEK
Many early breakdowns disappear, except one Z3
p/n difference explained by the fluences (10,13)

## Slide 6: I-V irradiated and breakdown
Pre-Series I: post-rad i-V @RT
Breakdown Pre-Series I: pre-rad / post-rad
Post-rad marked improvement of breakdown
0.15 x1014 p/cm2
Post-rad IV measured up to 800V

## Slide 7: Leak current (@500/800V)‏ after annealing
p/n damages contribute similarly to leakage current increase
measurements at different sites agree within uncertainties
4x10-17 A/cm
*1015 /cm2
*0.03 cm3 (:GEO=1)
*0.018 (: I-20/I20)
=22A
No surprise in damage!

## Slide 8: C-V irradiated after annealing
p13.2,n10.0(×1014)‏
p6.0,n5.0
proton z1
proton z3
proton z4
neutron z3
neutron z5
p2.1,n2.0
Pstop only
Pstop
+pspray
FDVs for neutron irradiated samples are apparently larger
Tsukuba/KEK
f=1kHz

## Slide 9: Full Depletion Voltages (from C-V)‏
from CV
from CV
Tsukuba/KEK
neutron
proton
proton

## Slide 10: Charge Collection Curves for FDV evaluation
neutrons may induce non-annealable “damages” which enhance laser interaction
Or, annealing is incomplete?
Tsukuba/KEK
measurement based on 1064 nm laser.
after 80 min at 60oC annealing
Evaluation of absolute CCE with laser is limited in precision for this wafer where pre-irradiation laser response is ~1/2 wrt conventional FZ.

## Slide 11: Full Depletion Voltages
(from C-V and CC curves)‏
FDVs evaluated from C-V and CC curves in agreement.
FDV evolution seems to quicker for neutron irradiation.
(damages are different. longer annealing necessary for n?)‏
Tsukuba/KEK

## Slide 12: Summary
Irradiation tests of ATLAS07 are being carried out
p-type FZ wafers (FZ_pure in ATLAS06) available to HPK are as good as n-type FZ in view of small initial leakage current and initial strip isolation (Z1 works, not covered here)
No surprise in leak current increase, full depletion voltage evolution (n contributes quicker to FDV evolution?), bulk annealing
FD or partial depleted operation remains an issue for charge collection time; Lorentz angle is being measured by Tsukuba/KEK group

## Slide 13
Proton Irradiation at CYRIC
Cyclotron (70 MeV: e.g. 8h for 1016/cm2 irradiation with 20cm2 scan )‏
BEAM profile @32line
Sample holder
samples
Profile monitor
<number>
Samples cooled to -10oC and biased,
scanned to perform uniform irradiation

## Slide 14
laser head
XY-stage
amps
collimators
focusing lens
Gamp=5mV/fC
Charge Collection Evaluation with Laser
Pulsed Nd:YAG(1064nm) laser can simulate passage of charge particle since it penetrates through Si. The above traces are for Fz samples irradiated to 0.2~5ｘ1015 n/cm2 (Vb=1kV)‏