## Slide 1: CVD diamond detector as a beam monitor for a high intensity and high luminosity accelerator
Kodai Matsuoka (Kyoto Univ.)
for T2K muon monitor group

## Slide 2: Contents
Introduction
  Motivation
Chemical Vapor Deposition (CVD) diamond
  Properties
  CVD diamond detectors in BaBar, Belle
  A candidate for T2K muon monitor
Beam test results of CVD diamond detectors
  Bias voltage scan
  Time dependence
  Linearity
Summary

## Slide 3: Motivation to study CVD diamond detector
A high intensity and high luminosity accelerator helps us to push back the frontiers in HEP.
Need more radiation-hard detectors
A new material tolerant of radiation:
Chemical Vapor Deposition (CVD) diamond
KEKB
Luminosity: 1034 cm-2 s-1
J-PARC
Intensity: 3.3 x 1014 proton / pulse

## Slide 4: CVD diamond
Formed by using a gas at low temp. (< 1000 °C) and low pressure (~0.1 atm) in a non-equilibrium process, Chemical Vapor Deposition (CVD) growth process.
Produced economically over a large area and w/ high purity.
Polycrystalline w/ a columnar structure of grains.
Schematic diagram of a CVD reactor
Scanning electron micrograph from the growth side of a CVD diamond sample
200 μm

## Slide 5: Properties of diamond
 | Diamond | Si
Band gap [eV] | 5.48 | 1.12
Electron mobility [cm2/Vs] | 2200 | 1450
Hole mobility [cm2/Vs] | 1600 | 500
Saturation velocity [cm/s] | 2 x 107 | 0.8 x 107
Dielectric constant | 5.7 | 11.9
e-h creation energy [eV] | 13 | 3.6
e-h pairs per MIP [μm-1] | 36 | 89
Displacement energy [eV] | 43 | 13 ~ 20
Decrease in charge collection after irradiation with 1 x 1015 proton/cm2 * | Not observed (by ~40 % at 5 x 1015 p/cm2) | No signal
Low leakage cur.
Low capacitance, noise
High radiation hardness
Fast signal collection
* CERN-EP/98-79 (1998)
Smaller signal (typically 1/5 of Si)
… Diamond is a better material than silicon

## Slide 6: CVD diamonds in BaBar
Photo of BaBar device inside SVT
CVD diamond
SVTRAD system
  Radiation monitoring and protection system to safeguard the Silicon Vertex Tracker (SVT)
  Two CVD diamonds were installed in Aug. 2002 to determine whether they presented a viable alternative to Si PIN photodiodes.
No operation problems
Lower noise than Si
Plan to replace all the Si PIN photodiodes w/ CVD diamonds
Cross-section view of SVT
Support ribs
Si PIN photodiode
Be beam pipe
Detector wafer

## Slide 7: CVD diamonds in Belle
Similar sensors as BaBar
Installed just outside of Silicon Vertex Detector (SVD)
CVD diamond has ever been no more than used as a radiation monitor.
The performance is not clear yet.
  Linearity
  Stability
  Reproducibility
  Individuality
CVD diamond
Photo of Belle device outside SVD

## Slide 8: T2K long baseline neutrino oscillation exp.
Super-K
295 km
J-PARC
~1 GeV νμ beam
Off-axis (OA)
It is necessary to monitor the ν direction. Muon monitor
Neutrino energy spectrum
Energy maximizing ν oscillation probability

## Slide 9: Muon monitor (MUMON)
Monitor of secondary beam direction by monitoring profile of muons which pass through beam dump on a spill by spill basis.
p
π+
μ+
νμ
MUMON baseline design:
an array of ionization chambers and an array of semiconductor detectors
Beam

## Slide 10: Requirements for MUMON system
Stability
Radiation hardness
# of particles coming into MUMON
    108 μ/cm2/spill
    107 neutron/cm2/spill
  (1000 times as much as in K2K MUMON)
A viable alternative to Si PIN photodiode is required for T2K MUMON.
A new candidate: CVD diamond detector
K2K MUMON:
an ionization chamber hodoscope and an array of Si PIN photodiode

## Slide 11: Beam test w/ electron LINAC @ Uji ICR
CVD diamond detector
Developed by
CERN RD42
Active area:
9.5 x 9.5 mm2
Thickness:
500 μm
9.5 mm
9.5 mm
Beam parameters
100 MeV electron
Intensity > 107 e/spill
Radius: ~2 cm
Pulse width: ~40 ns
Electron LINAC @ Inst. for Chem. Res. Kyoto Univ.
Si PIN photodiode (as a ref.)
10 mm
10 mm
HAMAMATSU
S3590-08
Active area:
10 x 10 mm2
Thickness:
300 μm

## Slide 12: Measured items
Bias voltage scan
Time dependence
Linearity
@ the flux expected in T2K MUMON
Beam profile
Beam
Diamonds
Si (as a ref.)
1 2 3
Schematic view of the test setup

## Slide 13: Bias voltage scan
The signal of diamond is ~1/5 of that of Si as expected.
Bias voltage dependence is < 0.1 %/V at 500 V.
Operation bias:
500 V
Beam intensity: ~5 x 107 e/cm2/pulse
Raw signal measured by oscilloscope
~80 ns
~800 ns
Diamond1 (bias: 500 V)
Si (bias: -80 V)
The diamond signal is faster than Si.

## Slide 14: Time dependence
Stable within 0.5 % for 10 min.
Beam intensity: ~5 x 107 e/cm2/pulse
< ± 0.5 %
Bias voltage on
Beam on
Pumping effect

## Slide 15: Linearity
The response of diamond is linear within 5.2 %.
Si seems to be saturated at the higher intensities.
Beam intensity: 107 ~ 108 e/cm2/pulse

## Slide 16: Summary
Intensity and luminosity frontiers has been improved.
  Radiation-hard detectors are required.
  CVD diamond is a new material tolerant of radiation.
CVD diamond detectors in BaBar, Belle
  Operated w/ no problem
  Should surpass performance of Si.
CVD diamond is a candidate for T2K MUMON.
  We succeeded in the beam test of CVD diamonds.
    Bias voltage dependence < 0.1 %/V at 500 V
    Stable within 0.5 % for 10 min.
    Linear response within 5.2 % up to 108 e/spill (T2K full intensity)
  There remain some issues to be considered.
    Individuality, Long-term stability, etc.
CVD diamond is involving in real alternative for detectors in extreme radiation environments.

## Slide 18: Supplement

## Slide 19: Main goals of T2K
Search for νe appearance, then determination of θ13
Precise measurement of oscillation parameters, θ23 and Δm232, by νμ disappearance
Search for sterile components in νμ disappearance
Expected sensitivities assuming 0.75MW and 170 days operation for five years
  νμ disappearance
    δ(Δm232) = 10-4 eV-2 • δ(sin22θ23) = 0.01
  Discovery of νμ νe
    Δm2 ~ 3 x 10-3 eV-2 • sin22θ13 ~ 0.006

## Slide 20: Off-axis (OA) neutrino beam
Off-axis ν flux at the desired energy is higher than on-axis flux.
  (Oscillation max. ~ 0.8 GeV for L = 295 km and Δm2 ~ 3 x 10-3 eV-2)
There are few high energy neutrinos which contribute not to the appearance signal but to its background.
Background due to intrinsic contamination of the beam by νe is less than at on-axis position.
Neutrino energy spectrum from OA beams

## Slide 21: CVD diamond results in BaBar
Fully correlated with nearby Si signal
Provide very clean signal due to their tiny dark currents
No operational problems
Radiation-induced cur. in CVD diamond detector and Si PIN photodiode during typical operation of the accelerator

## Slide 22: CVD diamond in K2K MUMON
Beam
K2K MUMON SSD-array
CVD diamond
Collected charge ratio of diamond / Si
= 13.8 pC / 160 pC
= 8.6 %

## Slide 23: Pumping effect
d(t) = dp [1 – r exp(-t / τ)]
Charge collection distance in irradiation with 90Sr source with an activity of 37Mrad
τ = 64 min.