## Slide 1: STJ development for cosmic background neutrino decay search
Yuji Takeuchi (Univ. of Tsukuba)
for SCD/Neutrino Decay Group
Dec. 10, 2013
DTP International Review @KEK

## Slide 2: Neutrino Decay Collaboration Members
As of Dec. 2013
Japan Group
Shin-Hong Kim, Yuji Takeuchi, Kenji Kiuchi, Kazuki Nagata,
Kota Kasahara, Tatsuya Ichimura, Takuya Okudaira, Masahiro Kanamaru,
Kouya Moriuchi, Ren Senzaki (University of Tsukuba),
Hirokazu Ikeda, Shuji Matsuura, Takehiko Wada (JAXA/ISAS),
Hirokazu Ishino, Atsuko Kibayashi, Yasuki Yuasa(Okayama University),
Takuo Yoshida, Shota Komura, Ryuta Hirose(Fukui University),
Satoshi Mima (RIKEN),
Yukihiro Kato (Kinki University) ,
Masashi Hazumi, Yasuo Arai (KEK)
US Group
Erik Ramberg, Mark Kozlovsky, Paul Rubinov, Dmitri Sergatskov,
Jonghee Yoo (Fermilab)
Korea Group
Soo-Bong Kim (Seoul National University)

## Slide 3: Motivation of -decay search in CB
Search for in cosmic neutrino background (CB)
  Direct detection of CB
  Direct detection of neutrino magnetic dipole moment
  Direct measurement of neutrino mass:
Aiming at sensitivity of detecting from decay for
  SM expectation
  Current experimental lower limit
  L-R symmetric model (for Dirac neutrino) predicts down to for - mixing angle
LRS: SU(2)LｘSU(2)RｘU(1)B-L
SM: SU(2)Lｘ U(1)Y
Suppressed by , GIM
Suppressed only by
1026 enhancement to SM
Neutrino magnetic moment term
PRL 38,(1977)1252, PRD 17(1978)1395

## Slide 4: Photon Energy in Neutrino Decay
m3=50meV
m1=1meV
m2=8.7meV
E =4.4meV
E =24meV
Sharp Edge with 1.9K smearing
Red Shift effect
dN/dE(A.U.)
(50m)
distribution in
meV]
From neutrino oscillation
From Planck+WP+highL+BAO
50meV<<87meV, 14~24meV
51~89m
E =24.8meV

## Slide 5: CIB and ZE Backgrounds to CB decay
AKARI
COBE
Zodiacal Light
Zodiacal Emission
Galaxy evolution model
Galactic dust emission
Integrated flux from galaxy counts
CMB
Sharp edge with 1.9K smearing and energy resolution of a detector(0%-5%)
Red shift effect
Expected spectrum
,
CIB (fit from COBE data)
CB decay
dN/dE(A.U.)
at (λ＝50μm)
Zodiacal Emission
~500nW/m2/sr
CIB (COBE)
~30nW/m2/s
-decay ()
~30nW/m2/s
-decay ()
~1pW/m2/s

## Slide 6: Detector requirements
Requirements for detector
  Continuous spectrum of photon energy around (, far infrared photon)
  Energy measurement for single photon with better than 2% resolution for to identify the edge in the spectrum
  Rocket and satellite experiment with this detector
Superconducting Tunneling Junction (STJ) detectors in development
  Array of 50 Nb/Al-STJ pixels with diffraction grating covering
    For rocket experiment aimed at launching in 2016 in earliest, aiming at improvement of lower limit for by 2 order
  STJ using Hafnium: Hf-STJ for satellite experiment (after 2020)
    : Superconducting gap energy for Hafnium
    for 25meV photon: if Fano-factor is less than 0.3

## Slide 7: STJ(Superconducting Tunnel Junction）Detector
A bias voltage V is applied across the junction.
A photon absorbed in the superconductor breaks Cooper pairs and creates tunneling current of quasiparticles proportional to the photon energy.
Superconducting / Insulator /Superconducting Josephson junction device

## Slide 8: STJ I-V curve
Sketch of a current-voltage (I-V) curve for STJ
The Cooper pair tunneling current (DC Josephson current) is seen at V = 0, and the quasi-particle tunneling current is seen for |V|>2
Josephson current is suppressed by magnetic field
Leak current
B field

## Slide 9
STJ energy resolution
Statistical fluctuation of number of quasiparticles is related to STJ energy resolution.
Smaller superconducting gap energy Δ yields better energy resolution
 | Si | Nb | Al | Hf
Tc[K] |  | 9.23 | 1.20 | 0.165
Δ[meV] | 1100 | 1.550 | 0.172 | 0.020
Δ: Superconducting gap energy
F: fano factor
E: Photon energy
Hf
Hf-STJ as a photon detector is not established
Nq.p.=25meV/1.7Δ=735
  2% energy resolution is achievable if Fano factor <0.3
Tc :SC critical temperature
Need ~1/10Tc for practical
operation
Nb
Well-established as Nb/Al-STJ
(back-tunneling gain from Al-layer)
Nq.p.=25meV/1.7Δ=9.5
Poor energy resolution, but photon counting is possible
Notes: 9

## Slide 10: Hf-STJ development
We succeeded in observation of Josephson current by Hf-HfOx-Hf barrier layer for the first time in the world in 2010
However, to use this as a detector, much improvement in leak current is required. ( is required to be at pA level or less)
B=10 Gauss
B=0 Gauss
HfOx：20Torr,1hour
anodic oxidation：45nm
Hf(350nm)
Hf(250nm)
Si wafer
A sample in 2012
200×200μm2
T=80~177mK
Ic=60μA
Ileak=50A@Vbias=10V
Rd=0.2Ω
By K. Nagata

## Slide 11: Hf-STJ Response to DC-like VIS light
20μV/DIV
50μA/DIV
Laser ON
Laser OFF
Oxidation on 30 Torr, 1 hour
Laser: 465nm, 100kHz
10uA/100kHz=6.2×108e/pulse
We observed Hf-STJ response to visible light
By K. Nagata
~10μA
V
I

## Slide 12
FIR single photon spectroscopy
with diffraction grating + Nb/Al-STJ array
  Diffraction grating covering (16-31meV)
Array of Nb/Al-STJ pixels: 50()x8()
  We use each Nb/Al-STJ cell as a single-photon counting detector with best S/N for FIR photon of
  for Nb: if consider factor 10 by back-tunneling
  Expected average rate of photon detection is ~350Hz for a single pixel
Need to develop ultra-low temperature (<2K) preamplifier
  In collaboration with Fermilab Milli-Kelvin Facility group (Japan-US collaboration: Search for Neutrino Decay)
  SOI-STJ in development with KEK
Nb/Al-STJ array
Assuming for STJ response time, requirements for STJ
Leak current <0.1nA
Need T<0.9K for detector operation
 Need to 3He sorption or ADR for the operation

## Slide 13: Temperature dependence of Nb/Al-STJ leak current
Temperature dependence
 10nA at T=0.9K
T=0.8K
B=40 Gauss
Rref=
If assume leak current is proportional to junction size, can achieve 0.1nA leak current to ~100 junction size
10nA @0.5mV
Need T<0.9K for detector operation
 Need to 3He sorption or ADR for the operation
Junction size: 100x100um2
13
This Nb/Al-STJ is provided by S. Mima (Riken)
100x100um2 Nb/Al-STJ I-V curve

## Slide 14: 100x100m2 Nb/Al-STJ response to NIR multi-photons
10 laser pulses in 200ns (each laser pulse has 56ps width
NIR laser through optical fiber
We observed a response to NIR photons
Response time ~1μs
Corresponding to 40 photons (Assuming incident photon statistics)
50μV/DIV
0.8μs/DIV
Observe voltage drop by 250μV
Response to NIR laser pulse（λ=1.31μm)
Signal pulse height distribution
Pedestal
Pulse height dispersion is consistent with ~40 photons
Pulse height (a.u.)
STJ
I
V
1k
T=1.8K
(Depressuring LHe)
Signal
By T. Okudaira

## Slide 15: 4m2 Nb/Al-STJ response to VIS light at single photon level
signal
pedestal
event
 Nγ=1.16±0.33
pulse height(a.u.)
4m2 Nb/Al-STJ response to two laser pulses (465nm)
Corresponding to 1.16±0.33 photons (Assuming incident photon statistics)
By T. Okudaira
Assuming photon statistics only
where
: mean of signal
: number of photons
: Gain (Vsig/N)
: sigma of pedestal
: sigma of signal

## Slide 16: 4m2 Nb/Al-STJ response to VIS light at single photon level
Best fit f(x;)
1photon
2photon
3photon
0photon
event
μ
x2
minimum at μ=0.93
ndf=85
pulse hight(AU)
Assuming a Poisson distribution convoluted with Gaussian which has same sigma as pedestal noise:
By T. Okudaira
Currently, readout noise is dominated, but we are detecting VIS light at single photon level

## Slide 17: 4m2 Nb/Al-STJ response to DC-like VIS light
0.5mV/div
20nA/div
I
V
VIS laser pulse (465nm) 20MHz illuminated on 4m2 Nb/Al-STJ
~10nA
10nA/20MHz=0.5×10-15 C =3.1×103 e
0.45 photons/laser pulse is given in previous slide
Laser OFF
Laser ON
Gain from Back-tunneling effect
Gal=6.7

## Slide 18: Development of SOI-STJ
SOI: Silicon-on-insulator
  CMOS in SOI is reported to work at 4.2K by T. Wada (JAXA), et al.
A development of SOI-STJ for our application with Y. Arai (KEK)
  STJ layer sputtered directly on SOI pre-amplifier
Started test with Nb/Al-STJ on SOI with p-MOS and n-MOS FET(w=1000um,L=1um)
SOI
STJ
Nb
metal pad
By K. Kasahara
STJ lower layer has electrical contact with SOI circuit
STJ
Gate
Drain
Source
STJ
Phys. 167, 602 (2012)

## Slide 19
KEK 超伝導検出器開発システム
Aligner
SOI wafer is manufactured by Lapis Semiconductor and STJ on SOI is formed at KEK cleanroom
Development of SOI-STJ
19

## Slide 20: Development of SOI-STJ
by K. Kasahara
2mV /DIV
1 mA /DIV
500uV /DIV
10 nA /DIV
2mV /DIV
50uA /DIV
2mV /DIV
1 mA /DIV
We formed Nb/Al-STJ on SOI
Josephson current observed
Leak current is 6nA @Vbias=0.5mV, T=700mK
B=0
B=150 gauss
n-MOS
p-MOS
n-MOS and p-MOS in SOI on which STJ is formed
Both n-MOS and p-MOS works at T=750~960mK
VGS[V]
0.7V
-0.7V
IDS[A]

## Slide 21
SOI上のNb/Al-STJの光応答信号
Pedestal
Signal
Iluminate 20 laser pulses (465nm, 50MHz) on 50x50um2 STJ which is formed on SOI
Estimated number of photons from output signal pulse height distribution assuming photon statistics
Nγ = ~ 206±112
500uV /DIV.
1uS /DIV.
Noise
Signal
M : Mean
σ : signal RMS
σp : pedestal RMS
Confirmed STJ formed on SOI responds to VIS laser pulses
STJ on SOI response to laser pulse

## Slide 22: Summary
We propose an experiment to search for neutrino radiative decay in cosmic neutrino background
We are developing a detector to measure single photon energy with <2% resolution for .
  Nb/Al-STJ array with grating and Hf-STJ are being considered
We’ve confirmed to SIS structure in our Hf-STJ prototypes
  Much improvement in leakage current is required for a practical use
We observed Nb/Al-STJ response to VIS light at single photon level, but readout noise is currently dominated.
Development of readout electronics for Nb/Al-STJ is underway
  As the first milestone, aiming to single VIS/NIR photon counting
  Several ultra low temperature amplifier candidates are under development. SOI-STJ is one of promising candidates

## Slide 23: Backup

## Slide 24: Energy/Wavelength/Frequency

## Slide 25: Cosmic neutrino background (CB)
CMB
CB

## Slide 26: STJ back tunneling effect
Photon
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb/Al-STJ Nb(200nm)/Al(10nm)/AlOx/Al(10nm)/Nb(100nm)
Gain: 2～200
Nb
Al
Nb
Al

## Slide 27: Feasibility of VIS/NIR single photon detection
Assume typical time constant from STJ response to pulsed light is ~1μs
Assume leakage is 160nA
Fluctuation from electron statistics in 1μs is
While expected signal for 1eV are
(Assume back tunneling gain x10)
  More than 3sigma away from leakage fluctuation

## Slide 28: Feasibility of FIR single photon detection
Assume typical time constant from STJ response to pulsed light is ~1μs
Assume leak current is 0.1nA
Fluctuation due to electron statistics in 1μs is
While expected signal charge for 25meV are
(Assume back tunneling gain x10)
  More than 3sigma away from leakage fluctuation
Requirement for amplifier
    Noise<16e
    Gain: 1V/fC  V=16mV