## Slide 1: Search for Cosmic Background Neutrino Decay with STJ detectors
Yuji Takeuchi (Univ. of Tsukuba)
Aug. 27, 2013
MKIDs and Cosmology workshop
Fermilab WH3NW
Contents
Motivation
STJ development
  Hf-STJ
  Nb/Al-STJ response
  SOI-STJ

## Slide 2: Collaboration Members (Japan-US collab.: Search for Neutrino Decay)
As of Aug. 2013
Japan Group
Shin-Hong Kim, Yuji Takeuchi, Kenji Kiuchi, Kanai, Kazuki Nagata,
Kota Kasahara, Tatsuya Ichimura, Takuya Okudaira, Kouya Moriuchi,
Ren Senzaki (University of Tsukuba),
Hirokazu Ikeda, Shuji Matsuura, Takehiko Wada (JAXA/ISAS) ,
Hirokazu Ishino, Atsuko Kibayashi, Yasuki Yuasa(Okayama University) ,
Takuo Yoshida, Yusuke Shimizu, Mikiya Nagashima (Fukui University) ,
Satoshi Mima (RIKEN),
Yukihiro Kato (Kinki University) ,
Masashi Hazumi, Yasuo Arai (KEK)
US Group
Erik Ramberg, Mark Kozlovsky, Paul Rubinov, Dmitri Sergatskov, Jonghee Yoo (Fermilab)
Korea Group
Soo-Bong Kim (Seoul National University)

## Slide 3: Cosmic neutrino background (CB)
CMB
CB

## Slide 4: Motivation
Search for in cosmic neutrino background (CB)
  Direct detection of CB
  Direct detection of neutrino magnetic moment
  Direct measurement of neutrino mass:
Aiming at sensitivity of detecting from decay for
  Current experimental lower limit
  SM expectation
  L-R symmetric model (for Dirac neutrino) predicts
LRS: SU(2)LｘSU(2)RｘU(1)B-L
SM: SU(2)Lｘ U(1)Y
Suppressed by , GIM
Suppressed only by
1026 enhancement to SM
Neutrino magnetic moment term
PRL 38,(1977)1252, PRD 17(1978)1395

## Slide 5: Photon Energy in Neutrino Decay
m3=50meV
m1=1meV
m2=8.7meV
E =4.4meV
E =24meV
Sharp Edge with 1.9K smearing
Red Shift effect
dN/dE(A.U.)
distribution in
meV]
From neutrino oscillation
From CMB fit (Plank+WP+highL+BAO)
50meV<<87meV, 14~24meV
51~89m

## Slide 6: Feasibility of photon detection from CB decay
Zodiacal Light
Zodiacal Emission
Surface brightness
Galactic dust emission
Wavelength[m]
Integrated flux from galaxy counts
Galaxy evolution model
CIB measurements( AKARI,  COBE)
Astrophys. J. 737 (2011) 2
Sharp edge with 1.9K smearing and energy resolution of a detector(0%-5%)
Red shift effect
Expected spectrum: and
CIB (fit from COBE data)
Differential photon energy spectrum from CB decay + CIB (w/ 2% energy resolution)
Statistical uncertainties in are taken into account in the error bars
(eV)
CB decay
6.7 away from flat
Simulation(JPSJ 81 (2012) 024101)
If we assumed
  and r
  No zodiacal foreground emission
  10 hour measurement
  20cm diameter and 0.1o viewing angle telescope
  A photon detector with 2% energy resolution
We can detect photon from CB decay photon at 6.7 significance

## Slide 7: Neutrino lifetime lower limit from AKARI data
x1012 yr
Fit CIB data to spectrum expected from decay assuming all contribution to CIB is only from decay
lifetime lower limit as a function of
Published in Jan. 2012
AKARI CIB data after subtracting foregrounds
Best fit spectrum from CB decay

## Slide 8: Detector requirements
Requirements for detector
  Energy measurement for single photon with better than 2% resolution for (, far infrared photon)
  Rocket and satellite experiment with this detector
Superconducting Tunneling Junction (STJ) detectors in development
  Array of 50 Nb/Al-STJ pixels with diffraction grating covering
    For rocket experiment aimed at launching in 2016 in earliest, aiming at improvement of lower limit for by 2 order
  STJ using Hafnium: Hf-STJ for satellite experiment (after 2020)
    : Superconducting gap energy for Hafnium
    for 25meV photon: if Fano-factor is less than 0.3

## Slide 9
Energy resolution of STJ
Energy resolution of STJ is limited by fluctuation of number of quasi-particles
Smaller superconducting gap energy gives better energy resolution
 | Si | Nb | Al | Hf
Tc[K] |  | 9.23 | 1.20 | 0.165
Δ[meV] | 1100 | 1.550 | 0.172 | 0.020
Hc[G] |  | 1980 | 105 | 13
Δ: Gap energy
F: Fano factor
E: Incident photon energy
In case of Hf, number of quasi-particles is N=25meV/1.7Δ=735
  % ＠25meV
  If Fano factor <0.3, 2% energy resolution is achievable
Tc :Critical temperature
  STJ operation temperature: 1/10 TC
Hc :Critical magnetic field
Energy resolution of STJ
In case of Nb, N=9.5
No report on practical Hf-STJ in the world
Notes: 9

## Slide 10: Hf-STJ development
We succeeded in observation of Josephson current by Hf-HfOx-Hf barrier layer for the first time in the world in 2010
However, to use this as a detector, much improvement in leak current is required. ( is required to be at pA level or less)
By K. Nagata
B=10 Gauss
B=0 Gauss
HfOx：20Torr,1hour
anodic oxidation：45nm
Hf(350nm)
Hf(250nm)
Si wafer
A sample in 2012
200×200μm2
T=80~177mK
Ic=60μA
Ileak=50A@Vbias=10V
Rd=0.2Ω

## Slide 11
Far Infrared Photon Spectroscopy with
Diffraction Grating + Nb/Al-STJ Array
  Diffraction grating covering (16-31meV)
Array of Nb/Al-STJ pixels
  We use each Nb/Al-STJ pixel as a single-photon counting detector with extremely good S/N for FIR photon of
  for Nb: (assuming x10 for back-tunneling gain)
  Expected average rate of photon detection is ~12kHz for a single pixel
Developing ultra-low temperature preamplifier to achieve noise<16e with Fermilab group
Nb/Al-STJ array
Assuming for STJ response time, for 25meV single photon counting
STJ leak current <0.1nA

## Slide 12: Temperature dependence of Nb/Al-STJ leak current
Temperature dependence
 10nA at T=0.9K
T=0.8K
B=40 Gauss
Rref=
If assume leak current is proportional to junction size, can achieve 0.1nA leak current to ~100 junction size
10nA @0.5mV
Need T<0.9K for detector operation
 Need to 3He sorption or ADR for the operation
Junction size: 100x100um2
12
This Nb/Al-STJ is provided by S. Mima (Riken)
100x100um2 Nb/Al-STJ I-V curve

## Slide 13: Nb/Al-STJ response to NIR photons
10 laser pulses in 200ns (each laser pulse has 56ps width
NIR laser through optical fiber
We observed a response to NIR photons
Response time ~1μs
Corresponding to 40 photons (Assuming incident photon statistics)
Back-tunneling gain 45 (assuming 40 photons corresponds 120fC)
50μV/DIV
0.8μs/DIV
Observe voltage drop by 250μV
Response to NIR laser pulse（λ=1.31μm)
Signal charge distribution
Pedestal
Signal charge dispersion is consistent with ~40 photons
Charge（pC)
by T. Okudaira
STJ
I
V
1k
T=1.8K
(Depressuring LHe)
Signal
120fC

## Slide 14: Development of SOI-STJ
SOI: Silicon-on-insulator
  CMOS in SOI is reported to work at 4.2K by T. Wada (JAXA), et al.
A development of SOI-STJ for our application with Y. Arai (KEK)
  STJ layer sputtered directly on SOI pre-amplifier
Started test with Nb/Al-STJ on SOI with p-MOS and n-MOS FET
SOI
STJ
Nb
metal pad
By Kota Kasahara
STJ lower layer has electrical contact with SOI circuit
STJ
Gate
Drain
Source
STJ
Phys. 167, 602 (2012)

## Slide 15: Development of SOI-STJ
by K. Kasahara
2mV /DIV
1 mA /DIV
500uV /DIV.
10 nA /DIV.
2mV /DIV.
50uA /DIV.
2mV /DIV
1 mA /DIV
We formed Nb/Al-STJ on SOI
Josephson current observed
Leak current is 6nA @Vbias=0.5mV, T=700mK
B=0
B=150 gauss
n-MOS
p-MOS
n-MOS and p-MOS in SOI on which STJ is formed
Both n-MOS and p-MOS works at T=750~960mK
VGS[V]
0.7V
-0.7V
IDS[A]

## Slide 16: Summary
We propose an experiment to search for neutrino radiative decay in cosmic neutrino background
  There is some chance to observe to neutrino radiative decay if we assume L-R symmetric model
We are developing a detector to measure single photon energy with <2% resolution for .
  Nb/Al-STJ array with grating and Hf-STJ are being considered
We’ve confirmed to SIS structure in our Hf-STJ prototypes
  Much improvement in leakage current is required for a practical use
Development of readout electronics for Nb/Al-STJ is underway
  As the first milestone, aiming to single NIR photon counting
  Several ultra low temperature amplifier candidates are under development. SOI-STJ is one of promising candidates

## Slide 17: Backup

## Slide 18: Energy/Wavelength/Frequency

## Slide 19: Feasibility of FIR single photon detection
Assume typical time constant from STJ response to pulsed light is ~1μs
Assume leak current is 0.1nA
Fluctuation due to electron statistics in 1μs is
While expected signal charge for 25meV are
(Assume back tunneling gain x10)
  More than 3sigma away from leakage fluctuation