## Slide 1: STJ developments for FIR photon spectroscopy at Tsukuba
Yuji Takeuchi (Univ. of Tsukuba)
Aug. 20, 2013
SCD review @ KEK 2-Go-kan Bldg.
Contents
Motivation
Hf-STJ development
Nb/Al-STJ response
Development Nb/Al-STJ readout
  FNAL test/SOI opamp/SOI-STJ

## Slide 2: Collaboration Members (Japan-US collab.: Search for Neutrino Decay)
As of Aug. 2012
Japan Group
Shin-Hong Kim, Yuji Takeuchi, Kenji Kiuchi, Kanai, Kazuki Nagata,
Kota Kasahara, Ryuuya Ichimura, Takuya Okudaira, Kouya Moriuchi,
Ren Senzaki (University of Tsukuba) ,
Hirokazu Ikeda, Shuji Matsuura, Takehiko Wada (JAXA/ISAS) ,
Hirokazu Ishino, Atsuko Kibayashi, Yasuki Yuasa(Okayama University) ,
Takuo Yoshida, Yusuke Shimizu, Mikiya Nagashima (Fukui University) ,
Satoshi Mima (RIKEN),
Yukihiro Kato (Kinki University) ,
Masashi Hazumi, Yasuo Arai (KEK)
US Group
Erik Ramberg, Mark Kozlovsky, Paul Rubinov, Dmitri Sergatskov, Jonghee Yoo (Fermilab)
Korea Group
Soo-Bong Kim (Seoul National University)

## Slide 3
Neutrino Decay Search 関連の成果 JFY2012~
Proceedings
  S. Kim et al., TIPP2011 Physics Procedia 37(2012)667-674
学会発表
  京都産業大学(2012年9月) ： 金井
  東広島学会(2013年3月)： 永田，笠原
APPC12(2013年7月): 金
CMB2013(2013年6月): ポスターセッション(武内，笠原，奥平)
SPICA collaboration 2013 (2013年6月): ポスターセッション(金)
「背景放射で拓く宇宙創成の物理]シンポジウム2012(2012年7月)：武内
「ニュートリノフロンティアの融合と進化」研究会(2013年4月)：金
SATテクノロジーショーケース(2013年1月)：金井(他)

## Slide 4: Motivation
Search for in cosmic neutrino background (CB)
  Direct detection of CB
  Direct detection of neutrino magnetic moment
  Direct measurement of neutrino mass:
Aiming at sensitivity of detecting from decay for
  Current experimental lower limit
  SM expectation
  L-R symmetric model (for Dirac neutrino) predicts
L-R: SU(2)LｘSU(2)RｘU(1)B-L
SM: SU(2)Lｘ U(1)Y
Suppressed by , GIM
Suppressed only by
1026 enhancement from SM
Neutrino magnetic moment term
PRL 38,(1977)1252, PRD 17(1978)1395

## Slide 5: Feasibility of photon detection from CB decay
Simulation(JPSJ 81 (2012) 024101)
If we assumed
  No zodiacal emission background
  10 hour measurement
  20cm diameter and 0.1o viewing angle telescope
  A photon detector with 2% energy resolution
We can detect CB decay photon for and at 6.7 significance.
Zodiacal Light
Zodiacal Emission
Surface brightness
Galactic dust emission
Wavelength[m]
Integrated flux from galaxy counts
galaxy evolution model
CIB measurements( AKARI,  COBE) Astrophys. J. 737 (2011) 2
Sharp edge with 1.9K smearing and energy resolution of a detector(0%-5%)
Red shift effect
Expected spectrum for and
CIB (fit from COBE data)
Differential photon energy spectrum from CB decay + CIB (w/ 2% energy resolution)
Statistical uncertainties in are taken into account in the error bars
(eV)
CB decay
6.7

## Slide 6: Detector requirements
Requirements for detector
  Energy measurement for single photon with better than 2% resolution for (, far infrared photon)
  Rocket and satellite experiment with this detector
Superconducting Tunneling Junction (STJ) detectors in development
  Array of 50 Nb/Al-STJ cell with diffraction grating covering
    For rocket experiment aimed at launching in 2016 in earliest, aiming at improvement of lower limit for by 2 order
  STJ using Hafnium: Hf-STJ for satellite experiment (after 2020)
    : Superconducting gap energy for Hafnium
    for 25meV photon: if Fano-factor is less than 0.7 (No gain from back tunneling effect is assumed)

## Slide 7: Hf-STJ development
We succeeded in observation of Josephson current by Hf-HfOx-Hf barrier layer for the first time in the world in 2010.
@T=120-130mK
However, to use this as a detector, much improvement in leak current is required. ( is required to be at pA level or less)
Oxidative condition
1 hour in 10Torr Oxygen ambience
250nm
250nm
木内修論

## Slide 8: Hf-STJ development
For several Hf-STJ samples on the following conditions, we observed Josephson current
Hf(350nm)
Hf(250nm)
Si wafer
HfOx：20Torr,1hour
anodic oxidation：45nm
Wafer Label | Chip # | Junction ID | Junction size | Oxidation O2 press. | Inverse sputtering
HfA | 1 | j0 | 200x200μm2 | 20 Torr | 
 |  | j1 | 100x100μm2 | 20 Torr | 
 |  | j2 | 100x100μm2 | 20 Torr | 
 | 2 | j0 | 200x200μm2 | 20 Torr | 
HfA_30 | 2 | j0 | 200x200μm2 | 30 Torr | 
 | 1 | j3 | 100x100μm2 | 30 Torr | 
HfB | 1 | j0 | 200x200μm2 | 20 Torr | 
Chip #
By Kazuki Nagata

## Slide 9: Examples of I-V curve measurement of Hf-STJ in JFY2012
B=10 Gauss
HfA2 j0: 200×200μm2
T=80~177mK
Ic=60μA Rd=0.2Ω
HfA1 j2: 100×100μm2
T=39~53mK
Ic=10μA Rd=0.6Ω
B=0 Gauss
B=0 Gauss
B=10 Gauss
永田修論
I-V curve with averaging

## Slide 10
Other I-V curves (w/ Magnetic field of ~10 Gauss)
Junction ID | Rd (Ω)
HfA1(j0) | 0.26
HfA2(j0) | 0.20
HfA1(j1) | 0.35
HfA1(j2) | 0.60
HfA_302(j0) | 0.20
HfA_301(j3) | 0.85
HfB1(j0) | 0.03
HfA1:j0
HfA2:j0
HfA1:j1
HfA1:j2
HfA_302:j0
HfA_301:j3
HfB1:j0
Samples with smaller junction size
Smaller leak current (Larger Rd)
By Kazuki Nagata
100×100μm2

## Slide 11: I-V curves (w/ B field, w/o averaging)
Junction ID | Noise (μA)
HfA1(j0) | 100
HfA2(j0) | 180
HfA1(j1) | 100
HfA1(j2) | 60
HfA_302(j0) | 160
HfA_301(j3) | 40
HfB1(j0) | >300
HfA1(j0)
HfA2(j0)
HfA1(j1)
HfA1(j2)
HfA_302(j0)
HfA_301(j3)
HfB1(j0)
Noise in current measurement is correlated with junction size
Probably, correlated with STJ capacitance
By Kazuki Nagata

## Slide 12: Summary of Hf-STJ samples
Junction ID | Junction size | Rd (Ω) | Ic (μA) | Noise (μA)
HfA1 (j0) | 200×200μm2 | 0.26 | 10 | 100
HfA2 (j0) | 200×200μm2 | 0.2 | 60 | 180
HfA1 (j1) | 100×100μm2 | 0.35 | 10 | 100
HfA1 (j2) | 100×100μm2 | 0.6 | 10 | 60
HfA_302 (j0) | 200×200μm2 | 0.2 | 30 | 160
HfA_301 (j3) | 100×100μm2 | 0.85 | 10 | 40
HfB1 (j0) | 200×200μm2 | 0.03 | 80 | >300
Smaller junction size
  Smaller leak current (larger Rd)
  Magnitude of noise in current measurement seems to be correlated with junction size (i.e. STJ capacitance)
Inverse sputtering before HfOx layer → No good
O2 pressure for HfOx oxidation → No significant difference between 20 Torr and 30 Torr cases
By Kazuki Nagata

## Slide 13: Temperature dependence of Rd
T= 55 mK
T=104 mK
T=180 mK
T=230 mK
Rd is increasing as lower temperature
Below 104mK, Rd increase is saturated.
HfA_301 j3 (100×100μm2)
B=10 Gauss
T (mK) | Rd (Ω)
230 | 0.50
180 | 0.56
104 | 0.80
55 | 0.80
230mK is close to Tc of this sample
By Kazuki Nagata

## Slide 14: HfOx layer with Electron Energy-Loss Spectroscopy(EELS)
O atom intensity (arb.)
0nm
10nm
HfA (Oxidation on 20 Torr, 1 hour)
0nm
12nm
For both cases, about 2nm oxidation layers are observed.
2nm
2nm
HfA_30 (Oxidation on 30 Torr, 1 hour)
O atom intensity (arb.)

## Slide 15: Hf-STJ のDC光に対する応答
20μV/DIV
50μA/DIV
永田2013/4/2
青色レーザーON
青色レーザーOFF
HfA_30 (Oxidation on 30 Torr, 1 hour)
Laser: 465nm, 100kHz

## Slide 16: Hf-STJのパルス光に対する応答
光照射なし
光照射あり
40 μS/DIV
10 μV/DIV
レーザーパルストリガー
レーザーパルストリガー
永田2013/4/2
これが本当にSTJとしての光応答なのか，定量的な議論は今のところ全くなし．Hf-STJの何らかの光応答を見たのは，おそらく世界初だろう…

## Slide 17: Summary on Hf-STJ development
Now we have several Hf-STJs in which we can observe Josephson current.
We’ve begun to investigate leakage current in Hf-STJ systematically from I-V curve measurements.
We want to measure I-V curve in lower noise environment from readout electronics as possible.
In parallel to I-V measurement, we’ve started measuring Hf-STJ response to light (pulse) incident.
  We want to use an ultra-low temperature amplifier which is being developed for Nb/Al-STJ if available.
Plan

## Slide 18
FIR photon spectroscopy with
diffraction grating + Nb/Al-STJ array
  Diffraction grating covering (16-31meV)
Array of Nb/Al-STJ cell
  We use each Nb/Al-STJ cell as a single-photon counting detector with extremely good S/N for FIR photon of
  for Nb: if consider factor 10 by back-tunneling
  Expected average rate of photon detection is about 12KHz for a single cell
Need to develop ultra-low temperature (2K) preamplifier
  In collaboration with Fermilab Milli-Kelvin Facility group (Japan-US collaboration: Search for Neutrino Decay)
Nb/Al-STJ array
Assuming for STJ response time, requirements for STJ
Leak current <0.1nA

## Slide 19: Temperature dependence of Nb/Al-STJ leak current
Temperature dependence
 10nA at T=0.9K
T=0.8K
B=40 Gauss
Rref=
If we assume leak current proportional to junction size,
We can achieve 0.1nA in leak current for ~100 in junction size
10nA @0.5mV
Need T<0.9K for detector operation
 Need to consider 3He sorption or ADR refrigerator toward the final goal
Junction size: 100x100um2
By Shinya Kanai
19
This Nb/Al-STJ is provided by Mima-san (Riken)

## Slide 20: Nb/Al-STJ 赤外光応答信号
STJ
1k
I
V
Read
Read
レーザーパルス幅 56ps パルス間隔20ns
10パルス照射(200ns幅パルス相当）
T=1.8K
(He減圧冷凍機）
赤外線レーザー(光ファイバーで入射）
赤外光応答信号を観測
応答速度～１μs
40photon相当(photon statisticsを仮定)
逆に40photonを仮定すると信号電荷(120fC)からは，trapping gain が45
50μV/DIV
0.8μs/DIV
250μVの電圧変化を確認
赤外線レーザー（λ=1.31μm)に対する応答信号
信号電荷分布
ペデスタル
分布の広がりから
光子数~40 photons
信号電荷（pC)
by T. Okudaira

## Slide 21: SOI-STJ
Gate
Drain
Source
STJ
ViaによるSOI回路層と
STJの電気的接触接触
STJ検出器のノイズに対する読み出し系の改善
SOIのLSI化の技術
エネルギー分解能の高いSTJ検出器
SOI-STJとは…
電荷積分アンプが形成されたSOIの回路層に直接STJを形成。
現在はMOSFET単体とNb/Al-STJによる試作を性能評価を行っている．
SOI-STJの利点
STJ検出器から配線の引き回しが不要。
良いS/N比
STJのマルチチャンネル化に対応可能。
STJ
by K. Kasahara

## Slide 22: SOI-STJ研究開発の現状
2.9mm角 SOI-STJ Layout
Wire Bonding
V+
I+
V-
I-
16個のpatternの内、SOIFETの形成されていないpatternを使用して、希釈冷凍機による700mKでのNb/Al-STJの性能評価を行った。
Refrigerator
SOI上の形成したNb/Al-STJでジョセフソン接合素子特有のI-V特性を確認。
Leak Current at 0.5mV
~6nA
約150 Gauss印加
2mV /DIV.
1 mA /DIV.
500uV /DIV.
10 nA /DIV.
2mV /DIV.
50uA /DIV.
2mV /DIV.
1 mA /DIV.
1K Ohm
by K. Kasahara

## Slide 23: SOI-STJ研究開発の現状
STJの正常な動作を確認したものと同chip上のMOSFETが熱励起によるリークカレントが起こらなくなる1K以下の領域で正常に動作する事を確認。
STJ leak currentは熱励起によるもの、不完全なJunctionの形成によるものの2つあると考えられる。
現在使用しているSiwaferに直接Nb/Al-STJを形成したものでは左図のleak currentの温度依存性が見られた。
Nb/Al-STJ Leak Current
SOI-STJはリークの最も小さくなる1K以下での動作を目指すため、SOIFETは1K以下で動作することが要求される。
by K. Kasahara

## Slide 24: SOISTJ2 layout for next SOI process
SOI-STJ
Vgsをモニター
C1
R1
C2
1photon : 300 uV
2photon : 700 uV
3photon : 1 mV
中赤外光入射の際の回路シミュレーション
Al layer trapping gain= 10 を仮定
, ,
STJの擬似信号電流
2S
by K. Kasahara

## Slide 25: Summary
We are developing a detector to measure single photon energy with <2% resolution for .
  Our choices are Hf-STJ and Nb/Al-STJ array with grating.
We’ve confirmed to Hf-HfOx-Hf structure is established.
  Much improvement in leakage current is required.
  We start looking at Hf-STJ response to photons.
Development of readout electronics for Nb/Al-STJ is underway.
  Aiming to measure a single photon of visible/NIR light at the first milestone.
  Several ultra low temperature amplifier candidates are under development. SOI-STJ is one of promising candidates.

## Slide 26: Energy/Wavelength/Frequency

## Slide 27: Dilution refrigerator operation
Our record minimum temperature: 28mK
  4 samples, 1 optical fiber, and RuOx sensor are mounted on the stage
  RuOx sensor is calibrated at known Hf Tc (130mK)
  Goal for Hf-STJ operation: 20mK
28mK
Feb. 2012
Temperature(mK)
100
0
Resistance(Ω)
1
0
2
Hf wire
200
SC transition
Tc=130mK
The dilution refrigerator in this talk is provided by Prof. Ootuka (U. of Tsukuba)

## Slide 28: Feasibility of VIS/NIR single photon detection
Assume typical time constant from STJ response to pulsed light is ~1μs
Assume leakage is 160nA
Fluctuation from electron statistics in 1μs is
While expected signal for 1eV are
(Assume back tunneling gain x10)
  More than 3sigma away from leakage fluctuation

## Slide 29: Nb/Al-STJ 可視光応答信号
junction size STJ
Emission of 465nm pulsed light at single photon level
We estimated assuming photon stat.
Fit the charge distribution to the sum of distributions from 0, 1, 2, and 3 photons, assuming Poisson distribution for Nphoton distribution.
by T. Okudaira