## Slide 1: R&D of FIR quantum photo-sensors based on STJs for COBAND
TCHoU Workshop 2018
Feb. 4-5, 2019 / U. Tsukuba
Yuji Takeuchi (TCHoU, Univ. of Tsukuba)
for the COBAND collaboration

## Slide 2: COBAND(Cosmic Background Neutrino Decay)
Search for Neutrino decay in Cosmic background neutrino
To be observed as FIR photons around ~50m in the overwhelming zodiacal emission
time
Notes: 開発の動機となったものは，COBAND実験において宇宙背景ニュートリノのニュートリノ崩壊の探索というもので，
遠赤外領域で分光性能をもつ超高感度な光検出器が必要となります．

## Slide 3: Neutrino Decay signal and backgrounds
CMB
ISD
SL
DGL
CB decay
wavelength [m]
Surface brightness I [MJy/sr]
Zodiacal Emission
Zodiacal Light
Integrated flux from galaxy counts
CIB summary from Matsuura et al.(2011)
1000
100
10
1
0.0001
0.001
0.01
0.1
1
10
100
Zodiacal
Emission
Expected Neutrino
Decay signal
We can identify  decay signal by highly precise measurement of photon energy spectrum around ~50m
Current experimental lower limit is 1012 yrs

## Slide 4
Proposal of a rocket experiment
  Expect 200s measurement at altitude of 200~300km
  Combination of diffraction grating covering =40-80m and array of Nb/Al-STJ pixels: 50()x8()
  Aiming at launch in the early 2020’s and sensitivity to 1014 years
Nb/Al-STJ array
50()x8() array
Main mirror 15cmΦ
  Following the rocket experiment, a satellite experiment aiming at sensitivity to 1017 years is planned.
  We are developing Hf-STJ which is expected to have sufficient energy resolution to measure the spectrum without diffraction grating.

## Slide 5: Requirements for the photo-detector in COBAND rocket experiment

High detection efficiency for a far-infrared single-photon in =40m～80m
Dark count rate less than 300Hz (expected real photon rate)
We are trying to achieve by using
Superconducting Tunnel Junction (STJ) sensor
Cryogenic amplifier readout

## Slide 6: Superconducting Tunnel Junction (STJ) Sensor
A constant bias voltage (|V|<2) is applied across the junction.
A photon absorbed in the superconductor breaks Cooper pairs and creates tunneling current of quasi-particles proportional to the deposited photon energy.
Superconductor / Insulator /Superconductor Josephson junction device
Δ: Superconducting gap energy
2
E
Ns(E)
Superconductor
Superconductor
Insulator
Insulator
Superconductor
100m
300nm
Much lower gap energy (Δ) than FIR photon  Can detect FIR photon
Faster response (~s)  Suitable for single-photon counting

## Slide 7: STJ current-voltage curve
Optical signal readout
Apply a constant bias voltage (|V|<2) across the junction and collect tunneling current of quasi particles created by photons
Leak current causes background noise
Tunnel current of Cooper pairs (Josephson current) is suppressed by applying magnetic field
Leak current
B field
I-V curve with light illumination
Voltage
Current
Signal current

## Slide 8
STJ energy resolution for near infrared photon
P. Verhoeve et. al 1997
30m sq. Ta/Al-STJ
E~130meV @ E=620meV(=2m)
Charge sensitive amplifier at room temp.
  Electronic noise ~ 100meV
In sub-eV ~ several-eV region, STJ gives the best energy resolution among superconductor based detectors, but limited by readout electronic noise.
Photon Energy(eV)
FWHM(eV)
Electronic noise
Notes: 8

## Slide 9: Nb/Al-STJ development at CRAVITY
Temperature(K)
0.3
0.4
0.5
0.6
0.7
Leakage
100pA
1nA
10nA
100nA
Ileak~200pA for 50m sq. STJ, and achieved 50pA for 20m sq.
 This satisfies our requirement!
0.1nA
50m sq. Nb/Al-STJ fabricated at CRAVITY
500pA/DIV
0.2mV/DIV
I
V
T~300mK
w/ B field
Leakage
Far-infrared single photon detection is feasible with combination of Nb/Al-STJ sensor and cryogenic amplifier which can be deployed near the STJ.

## Slide 10: FD-SOI-MOSFET at cryogenic temperature
FD-SOI : Fully Depleted – Silicon On Insulator
Vgs (V)
Ids
0
0.5
1
1.5
2
1pA
1nA
1A
1mA
̶̶ ROOM
̶̶̶ 3K
n-MOS
p-MOS
̶̶ ROOM
̶̶̶ 3K
-Ids
1nA
1A
1mA
Vgs (V)
0
-0.5
-1
-1.5
-2
Id-Vg curve of W/L=10m/0.4m at |Vds|=1.8V
Both p-MOS and n-MOS show excellent performance at 3K and below.
~50nm
Channel Length : L
Channel Width : W
Very thin channel layer in MOSFET on SiO2
No floating body effect caused by charge accumulation in the body
FD-SOI-MOSFET is reported to work at 4K
    JAXA/ISIS AIPC 1185,286-289(2009)
    J Low Temp Phys 167, 602 (2012)
Increasement of drain current
Shift in VTH

## Slide 11: SOI prototype amplifier for demonstration test
Ｖ
Amplifier stage
Buffer stage
1nF
Test pulse
STJ
10M
3He sorption
cold stage
T~350mK
465nm laser pulse through optical fiber
GND
Vss
Vdd
4.7F
Cold amp. input monitor
Cold amp. output
STJ
SOI
4.7F
Voltage [μV]
70
60
50
40
18μV
Voltage [μV]
time [μs]
1600
1200
800
400
0
-100
-80
0
-40
-40
-20
20
40
60
80
100
1.2mV
Input to SOI amp. from STJ
Output from SOI amp.
Laser pulse(=465nm)
Demonstrated to show amplification of STJ response by SOI amplifier situated at T=350mK

## Slide 12
CC operation
Biasing STJ with large R keeps constant current on STJ
CV operation
STJ connection to virtual short through C keeps constant voltage on STJ
Read voltage by high input impedance amp.
STJ readout by
Constant Current and Constant Voltage operation
STJ
I
V
STJ I-V curve w/light w/o light
V0=V+RI
~1mV
Read charge by low input impedance amp.
Large fraction of fast component signal is lost through CSTJ
I
V
1mV
+
-
STJ
Better readout for STJ

## Slide 13: Charge sensitive amplifier
20μA
10μA
2μA
20μA
Buffer stage
40μA
Telescopic cascode current mirror
Feedback
Differential amp.
Negative feedback with C=3pF and R=5M
GBWP~2MHz
Differential amplifier with negative feedback of RC
Power consumption
~120W

## Slide 14: STJ response read with charge sensitive amplifier
Deploy STJ and SOI amp. on the cold stage in 3He sorption refrig.
Illuminate 465nm laser pulse onto the 20m sq. STJ.
Observed charge ~9fC corresponding to ~2photons
4.7F
Refrig.
-
+
1M
STJ
STJ chip
SOI chip
Optical fiber
fabricated at AIST/CRAVITY
Notes: 実証テストの成功を踏まえ，
STJ信号読み出しのための，より実際的な電荷積分型増幅器の作製および評価にも取り組んでおります．
こちらは，製作したSOI回路で，差動増幅回路に
キャパシタンスの負帰還をかけた電荷積分型増幅器となっています．
入力電荷に対して，室温と3ケルビンでほぼ同様の応答を確認しております．

## Slide 15: Hf-STJ development for future satellite experiment
We successfully made a device with SIS in 2010, and reduce leakage and observe response to laser pulse in 2017, but need to suppress leakage further down to ~pA for practical usage.
200m sq. in 2010
Hf-STJ(RMS=2.5nm)
200m200m
~25eV
T~140mK
200m sq. in 2017
10m sq. in 2018
Ileak~15A@20V
Ileak~7A@20V
Ileak~0.3A@20V
Since Hf has much smaller  (Hf =20eV) than Nb (Nb=1.5meV), Hf-STJ is expected to give much better energy resolution. However no group has succeeded in a practical Hf-STJ yet.

## Slide 16: Summary
In COBAND project, we require a photo-detector with NEP~10-19 W/Hz to detect single FIR photon (~50m) for the rocket experiment.
We are developing Nb/Al-STJ with cryogenic amplifier readout.
  Nb/Al-STJs fabricated at CRAVITY satisfy our requirements.
  Cryogenic FD-SOI amplifiers are under development and we demonstrated STJ signal amplification by a prototype SOI amplifier at T~350mK.
We are designing and testing more practical readout for STJ signal with low input impedance charge integration amplifier.
  Using SOI technology, a wealth of knowledge in circuit at room temperature is available even at cryogenic temperature almost as it is.
Hf-STJ is under development for future satellite experiment
* SOI design in this work is supported by VDEC, the U. Tokyo in collaboration with Synopsys, Inc., Cadence Design Systems, Inc., and Mentor Graphics, Inc.

## Slide 17: Backup

## Slide 18: COBAND (COsmic BAckground Neutrino Decay)
Heavier neutrinos in mass-eigenstate (2, 3) are not stable
  Neutrino can decay through the loop diagrams
However, the lifetime is expected to be much longer than the age of the universe
We search for neutrino decay using Cosmic Background Neutrino (CB) as the neutrino source

## Slide 19: Cosmic background neutrino (CB)
CMB
(=Photon decoupling)
~380,000yrs after the Big Bang
CB (=neutrino decoupling)
~1sec after the big bang

## Slide 20: Expected photon wavelength spectrum from CB decays
dN/d(a.u.)
[m]
100
500
10
Red Shift effect
Sharp Edge with 1.9K smearing
E [meV]
100
50
20
10
5
 distribution in
No other source has such a sharp edge structure!!
If assume
,
from neutrino oscillation measurements

## Slide 21: Motivation of -decay search in CB
If we observed the neutrino radiative decay at the lifetime much shorter than the SM expectation, it would be
Physics beyond the Standard Model
Direct detection of CB
Determination of the neutrino mass
Aiming at a sensitivity to 3 lifetime in
Standard Model expectation:
Experimental lower limit:
Left-Right symmetric model predicts for - mixing angle
3 Lifetime

## Slide 22: Existing FIR photo-detectors
Detectors | (μm) | Operation Temp. | NEP (W/Hz1/2) | 
Monolithic Ge:Ga | 50-110 | 2.2K | ～10-17 | Akari-FIS
Stressed Ge:Ga | 60-210 | 0.3K | ~0.9×10-17 | Herschel-PACS
Need more than 2 orders improvement from existing photoconductor-based detectors

## Slide 23
STJ energy resolution
Signal = Number of quasi-particles
Resolution = Statistical fluctuation in number of quasi-particles
Smaller superconducting gap energy Δ yields better energy resolution
Δ: Superconducting gap energy
F: fano factor (~0.2 for Nb)
E: Photon energy
G: Back-tunneling gain
Tc :SC critical temperature
Need ~1/10Tc for practical
operation
 | Si | Nb | Al | Hf
Tc[K] |  | 9.23 | 1.20 | 0.165
Δ[meV] | 1100 | 1.550 | 0.172 | 0.020
Notes: 23

## Slide 24: STJ back-tunneling effect
Photon
Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Quasi-particle near the barrier can mediate multiple Cooper pairs
Nb/Al-STJ Nb(200nm)/Al(70nm)/AlOx/Al(70nm)/Nb(200nm)
Gain: ～10
Nb
Al
Nb
Al
Si wafer
Nb
Nb
Al/AlOx/Al

## Slide 25: Drain Ａｖａｒａｎｃｈｅ
In the region of , drain current causes drastic increasement. We need to be care not to use this region in design.
0 0.5 1.0 1.5 2.0
0.6
0.5
0.4
0.3
0.2
0.1
0
-2.0 -1.5 -1.0 -0.5 0
0.3
0.2
0.1
0
curve (pmos)＠3K
W/L=10μm/5μm
curve (nmos)＠3K

## Slide 26: FET Threshold voltage control in Double-SOI at cryogenic temp.
We found Vth control is also possible at cryogenic temperature
Can compensate shift of Vth in cryogenic temp.
Can realize a FET with steep rising of Id around Vgs=0  Potential to ultra-low power consumption device
VDSOI
Middle silicon layer
BOX
pMOS-FET Id-Vgs curve
-1.5 -1 -0.5 0 0.5 Vgs(V)
1A
1nA
1pA
Id
Vth control by VDSOI at room temperature is well established.
3K