## Slide 1: Development of Superconducting Tunnel Junction Photon Detector with SOI Preamplifier board to Search for Radiative decays of Cosmic Background Neutrino
Tsukuba Global Science Week 2014
Takuya Okudaira1, Shinhong Kim1, Yuji Takeuchi1, Kota Kasahara1, Ren Senzaki1,Koya Moriuchi1 Kenichi Takemasa1, Kenji Kiuchi1, Tatsuya Ichimura1, Masahiro Kanamaru1, Hirokazu Ikeda2, Shuji Matsuura2, Takehiro Wada2, Hirokazu Ishino3, Atsuko Kibayashi3, Satoru Mima4, Takuo Yoshida5, Ryuta Hirose5, Yukihiro Kato6, Masashi Hazumi7, Yasuo Arai7 ,Erik Ramberg8, Jonghee Yoo8, Mark Kozlovsky8, Paul Rubinov8, Dmitri Sergatskov8, and Soo-Bong Kim9
University of Tsukuba1, JAXA/ISAS2, Okayama University3, RIKEN4 University of Fukui5, Kinki University6, KEK7 ,Fermilab8, Seoul National University9
Notes: I’d like to talk about development of STJ detector and SOI-STJ detector for Neutrino decay search

## Slide 2: STJ Detector
STJ(Superconducting Tunnel Junction) detector is
superconducting photoelectric detector that composed of
Superconductor / Insulator /Superconductor
~400nm
Nb
Al
AlOx
 | Si | Nb | Al
Tc [K] |  | 9.23 | 1.20
Δ [meV] | 1100 | 1.550 | 0.172
photon
quasiparticle
(electron)
cooper pair
insulator
Since energy gap of Nb is ~1meV (Si:~1eV), the energy resolution of STJ can be much better than semiconductor detector.
We are developing STJ photon detector for
neutrino decay search (as Dr. Takeuchi slide)
aiming at detecting single far infrared(50um) photon
Incident photons break up cooper pairs in STJ,
the electrons from the broken cooper pairs tunnel through the insulator layer
Notes: firstly I introduce STJ detector Superconducting tunnel junction is a superconducting photoelectric detector which consists of two superconducting layer separated by a very thin insulator layer .Incident Photons break up cooper pairs in STJ, the electrons from the broken cooper pairs go across the insulator layer and cause a current.

## Slide 3: Nb/Al-STJ
The signal to infrared(1310nm) laser
Typical signal width is about 1us
To achieve leakage current below 100pA…
Nb/Al-STJ is one of the candidate detector for neutrino decay search
Requirement for leakage current of
Nb/Al-STJ to detect single far infrared photon is below 100pA.
Because of this signal width
But we haven’t achieved such leakage current yet…
Temperature dependence of leakage current
with Nb/Al-STJ(100 x100um2)
use better quality STJ or smaller STJ
operate STJ below 800mK
Notes: We measured the response of Nb/Al-STJ (100umx100um) to near-infrared light Typical signal width of the signal was 1us at FWHM as shown in this picture. we are confirm leakage current saturates below 900mK

## Slide 4: STJ array prototype for Neutrino decay search
We processed STJ at AIST and KEK,
and measured distribution of infrared(1310nm) laser with STJ array
1.4mm
2.9mm
STJ array on the chip
The number of STJs : 10
The size of each STJ : 100um x100um
The distribution of infrared light with STJ array
The distribution of laser from fiber is
expected to be Gaussian
Red : Gaussian fit
Black : Output from each STJ
STJ illuminated with blue laser
STJ chip
carrier
laser fiber
STJ Output[AU]
Notes: We processed STJ at AIST and KEK, This chip is processed in AIST In this chip has STJ array like this. The number of STJ is 10, and The sizes of each STJ : 100um x100um
We measured the distribution of infrared light with STJ array. and we can get this plot. black points mean output from each STJs and we can fit this plot with Gaussian

## Slide 5: SOI-STJ
Silicon On Insulator (SOI)
Processing LSI on SiO2 insulator
Low Power to be operated
high speed
can operate at a few Kelvin
SOI-FET is suitable for amplifier for STJ signal
We are also developing a new detector :SOI-STJ
SOI-STJ
Processing STJ directly on a SOI preamplifier board to make the detector compact ,low noise and easy to be multipixel detector.
SOI-STJ can be new novel detector!
STJ
has high energy resolution
STJ processed on SOI
and schematic of prototype
Question
Is SOI caused any damage by processing STJ?
Can Nb/Al-STJ be processed on SOI board ?
Notes: The expected signal of single far-infrared photon with the Nb/Al-STJ is too small comparing with the present noise level of our readout electronics. SOI is Silicon On insulator that processed LSI on SIO2 insulator , the SOI has good properties. We combined these two technology into SOI-STJ. SOI-STJ is processed STJ directly on a SOI preamplifier board like this figure. this is Nb/Al-STJ, and this is connected to SOI-FET directly.
SO SOI-STJ doesn’t need any wire to connect from detector to preamplifier. According to this reason, SOI-STJ can be make the detector compact ,low noise and easy to process STJ into multipixel detector. And this picture is STJ processed on SOI board. there is this circuit on this picuture.

## Slide 6: STJ processed on SOI board
We confirmed STJ processed on SOI board has no problem!
apply magnetic
field
150 Gauss
2mV /DIV.
1 mA /DIV.
2mV /DIV.
50uA /DIV.
2mV /DIV.
1 mA /DIV.
500uV /DIV.
10 nA /DIV.
Signal of Nb/Al-STJ processed on SOI board to 465nm light
Leakage current : 6nA @0.5mV
We can process good
STJ on SOI board！
We observed typical STJ signal
from STJ on SOI board！
IV curve of the STJ on SOI board
Notes: SO we checked characteristic of STJ processed on SOI board. We can measure typical STJ IV curve like this. The leakage current of this STJ is 6nA, that means we can processed good STJ on SOI board.
this figure is signal of Nb/Al-STJ processed on SOI board to blue light.. In this picture we observed typical STJ signal from stj on SOI board. according to these things,, we confirmed STJ processed on SOI board has no problem

## Slide 7: SOI-FET after processing STJ at Low Temperature
NMOS(690~750mK)
PMOS(750mK)
Ids[A]
Vgs[V]
-Ids[A]
Vgs[V]
Vds[V]
gm[S]
Vds[V]
gm[S]
I-V curve of SOI-FETs after
processing Nb/Al-STJ.
Both of NMOS and PMOS
can be operated below 800mK.
Trans-conductance “gm” is
not varied drastically for each
temperature at operation
voltage(0.2V).
SOI-FET with STJ processed
has excellent performance
below 800mK.
SOI-FET is suitable for cold
preamplifier for STJ signal !
W=1000um
L=1um
W=1000um
L=1um
Notes: SO we checked the characteristic of SOI Transistor after processing STJ in low temperature. I-V curve of SOI-FETs after
processing Nb/Al-STJ at around 700mK. these result means SOI-FETs processing STJ has excellent performance in below 900mK.

## Slide 8: Summary
We are developing STJ and SOI-STJ to detect single
far infrared photon for neutrino decay search.
We confirmed
  STJ processed on SOI board has sufficient quality.
  SOI-FET has no damage by processing STJ
  SOI-FET has excellent performance below 800mK.

## Slide 9: BUCK UP

## Slide 10: Temperature dependence of IV curve

## Slide 11: Requirement for leakage current

## Slide 13
Division 1
100um×100um STJ array
Division 2
STJs with dispersed junction
Division 3
STJ array with
different sizes
Division 4
STJs with different under layer sizes
(Upper layer sizes are same )
To measure dispersion of quasi particle
Division 5
STJs with and without SiO2
To measure transmittance
of SiO2
Nb/Al-STJ on newly designed chip
Notes: new designed Nb/AL-STJ is this. There are 5 divisions,