## Slide 1: Search for neutrino radiative decay and the status of the far-infrared photon detector development
1st CiRfSE Workshop
Mar. 12-13, 2015 / University of Tsukuba, Japan
Yuji Takeuchi (Univ. of Tsukuba)
for Neutrino Decay Collaboration
S.H.Kim , K. Takemasa, K.Kiuchi , K.Nagata , K.Kasahara , T.Okudaira, T.Ichimura, M.Kanamaru, K.Moriuchi, R.Senzaki(Univ. of Tsukuba),
H.Ikeda, S.Matsuura, T.Wada(JAXA/ISAS),
H.Ishino, A.Kibayashi (Okayama Univ), S.Mima (RIKEN), Y.Kato (Kindai Univ.),
T.Yoshida, S.Komura, K.Orikasa, R.Hirose(Univ. of Fukui), Y.Arai, M.Hazumi (KEK),
S. Shiki, M. Ukibe, G. Fujii, T. Adachi, M. Ohkubo (AIST),
E.Ramberg, J.H.Yoo, M.Kozlovsky, P.Rubinov, D.Sergatskov (Fermilab),
S.B.Kim(Seoul National Univ.)

## Slide 2: Contents
Introduction to neutrino decay search
  Proposed rocket experiment
  Prospect for the neutrino decay search
Candidates for far-infrared single photon detector/spectrometer
  Nb/Al-STJ with diffraction grating
  Hf-STJ
Summary

## Slide 3: Neutrino
Neutrino has 3 mass generations (1, 2, 3)
Neutrino flavor states (e, , ) are not mass eigenstates
Neutrino flavor oscillates during the flight, and squared mass differences (, ) have been measured, but their absolute masses is not measured yet!
Neutrino can decay through the loop diagram
Neutrino lifetime is expected to be very long
use Cosmic neutrino background (CB) as the best neutrino source for neutrino decay search

## Slide 4: Cosmic neutrino background (CB)
CMB
CB (~1s after big bang)
The universe is filled with neutrinos.
But they are not detected yet!
Density (cm-3)

## Slide 5: Motivation of -decay search in CB
Search for in cosmic neutrino background (CB)
  Direct detection of CB
  Direct detection of transition magnetic dipole moment of neutrino
  Direct measurement of neutrino mass:
Aiming at sensitivity of detecting from decay for
  SM expectation
  Current experimental lower limit
  L-R symmetric model (for Dirac neutrino) predicts down to for - mixing angle
LRS: SU(2)LｘSU(2)RｘU(1)B-L
SM: SU(2)Lｘ U(1)Y
Suppressed by and GIM
Only suppressed by L-R mixing ()
1026 enhancement to SM
Magnetic moment term (L-R coupling)
PRL 38,(1977)1252, PRD 17(1978)1395

## Slide 6: Photon Energy in Neutrino Decay
m3=50meV
m1=1meV
m2=8.7meV
E =4.4meV
E =24meV
Sharp Edge with 1.9K smearing
Red Shift effect
dN/dE(a.u.)
distribution in
meV]
E =24.8meV
Two body decay
()
()
()
From neutrino oscillation
From Planck+WP+highL+BAO
50meV<<87meV
  14~24meV (51~89m)

## Slide 7: Backgrounds to CB decay
at λ＝50μm
Zodiacal Emission
~ 8 MJy/sr
CIB
~ 0.1-0.5 MJy/sr
~ 0.5MJy/sr
s
~ 25kJy/sr
Expected spectrum
CMB
ZE
ZL
ISD
SL
DGL
CB decay
wavelength [m]
E [meV]
Surface brightness I [MJy/sr]
AKARI
COBE
CB decay
λ＝50 μm
E=25 meV

## Slide 8: Detector requirements
Continuous spectrum of photon energy around 𝜆=50𝜇m (far infrared photon) with highly precise accuracy
  Photon-by-photon energy measurement with better than 2% resolution for (𝜆=50𝜇m ) to achieve better S/N as well as to identify the sharp edge in the spectrum
  A ground-based experiment is impossible, so rocket and/or satellite experiments with this detector are required
Superconducting Tunneling Junction (STJ) detectors in development
  Array of 50 Nb/Al-STJ pixels with diffraction grating covering
    For the rocket experiment aiming at improvement of current lower limit for by 2 order : O(1014 yrs) in a 200-sec measurement
  STJ using Hafnium: Hf-STJ for satellite experiment
    : Superconducting gap energy for Hafnium
    for 25meV photon: if Fano-factor is less than 0.3

## Slide 9: STJ(Superconducting Tunnel Junction）Detector
A bias voltage (|V|<2) is applied across the junction.
A photon absorbed in the superconductor breaks Cooper pairs and creates tunneling current of quasi-particles proportional to the photon energy.
Superconductor / Insulator /Superconductor Josephson junction device
Δ: Superconducting gap energy

## Slide 10: STJ examples
STJs are already in practical use as a single photon spectrometer for a photon ranging from near-infrared to X-ray, and show excellent performances comparing to conventional semiconductor detectors
5mm
5mm
H. Sato (RIKEN)
100mm x 100mm
5.9KeV X-ray
But no example for far-infrared photon so far

## Slide 11
STJ energy resolution
Statistical fluctuation in number of quasi-particles determines energy resolution
Smaller superconducting gap energy Δ yields better energy resolution
 | Si | Nb | Al | Hf
Tc[K] |  | 9.23 | 1.20 | 0.165
Δ[meV] | 1100 | 1.550 | 0.172 | 0.020
Δ: Superconducting gap energy
F: fano factor
E: Photon energy
Hf
Hf-STJ is not established as a practical photon detector
Nq.p.=25meV/1.7Δ=735
  2% energy resolution is achievable if Fano factor <0.3
Tc :SC critical temperature
Need ~1/10Tc for practical
operation
Nb
Well-established as Nb/Al-STJ
(back-tunneling gain from Al-layers)
Nq.p.=25meV/1.7Δ=9.5
Poor energy resolution, but photon counting is possible in principle
In both cases, developments are challenging
Notes: 11

## Slide 12
Proposal of a rocket experiment
  Expect 200s measurement at altitude of 200~300km
    Telescope with diameter of 15cm and focal length of 1m
    All optics (mirrors, filters, shutters and grating) will be cooled below 4K
  Diffraction grating covering =40-80m (16-31meV) and array of Nb/Al-STJ pixels: 50() x 8()
  Use each Nb/Al-STJ pixel as a single-photon counting detector for FIR photon of ()
  sensitive area of 100mx100m for each pixel (100rad x 100rad)
Nb/Al-STJ array

## Slide 13: Expected accuracy in the spectrum measurement
Telescope parameters
Main mirror
  D=15cm, F=1m
detector
  sensitive area 100mx100m/ pixel
  50 x 8 array
CMB
ISD
SL
DGL
CB decay
wavelength [m]
Surface brightness I [MJy/sr]
Zodiacal Emission
Zodiacal Light
  Zodiacal emission 343Hz / pixel
  200sec measurement: 0.55M events / 8 pixels (at )
  0.13% accuracy measurement for each wavelength: =11kJy/sr
Neutrino decay (, yrs): =25kJy/sr
  2.3σ away from statistical fluctuation in ZE measurement
Integrated flux from galaxy counts
 decay with yrs is possible to detect, or set lower limit!

## Slide 14: Sensitivity to neutrino decay
Parameters in the rocket experiment simulation
telescope dia.: 15cm
50 (: 40m – 80 m)  8 array
Viewing angle per single pixel: 100rad  100rad
Measurement time: 200 sec.
Photon detection efficiency: 100%
Can set lower limit on 3 lifetime at 4-6  1014 yrs if no neutrino decay observed
If 3 lifetime were 2  1014 yrs, can observe the signal at 5 significance level

## Slide 15: Status of Nb/Al-STJ photon detector development
Requirements for Nb/Al-STJ
Single photon detection for E=25meV (=50m)
  Detection efficiency: ~1
Dark count rate < 30Hz  STJ leak current < 0.1nA
Sensitive area: 100m  100m
Temperature [K]
Leak current [nA]
50m  50m Nb/Al-STJ fabricated at CRAVITY in AIST
Ileak<1nA achieved at AIST
We will try STJs with a smaller junction size
0.1nA
2.9mm

## Slide 16: 100x100m2 Nb/Al-STJ response to 465nm multi-photons
Laser pulse trigger
We observed a response of Nb/Al-STJs to NIR-VIS photons at nearly single photon level
Response time of STJ: O(1μs)
Due to the readout noise, we have not achieved FIR single photon detection
Need ultra-low noise readout system for STJ signal
2V/DIV
40μs/DIV
100x100m2 Nb/Al-STJ fabricated at CRAVITY
Dispersion of pulse height is consistent with 10~40-photon detection in STJ
465nm laser through optical fiber
STJ
10M
T~350m
(3He sorption)
Charge sensitive
pre-amp.
shaper amp.

## Slide 17: Development of SOI-STJ
SOI: Silicon-on-insulator
  CMOS in FD-SOI is reported to work at 4.2K by T. Wada (JAXA), et al.
A development of SOI-STJ for our application
  STJ layer is fabricated directly on SOI pre-amplifier and cooled down together with STJ
Started test with Nb/Al-STJ on SOI with p-MOS and n-MOS FET
SOI
STJ
Nb
metal pad
STJ lower layer has electrical contact with SOI circuit
Phys. 167, 602 (2012)
via
STJ
capacitor
FET
700 um
640 um
C
SOI-STJ2 circuit
D
S
G

## Slide 18: FD-SOI on which STJ is fabricated
Both nMOS and pMOS-FET in FD-SOI wafer on which a STJ is fabricated work fine at temperature down to ~100mK
We are also developing SOI-STJ where STJ is fabricated at CRAVITY
Charge sensitive pre-amplifier in SOI for STJ readout is also under development
B~150Gauss
2mV/DIV
1mA/DIV
I-V curve of a STJ fabricated at KEK on a FD-SOI wafer
Ids [A]
Vgs[V]
nMOS-FET in FD-SOI wafer on which a STJ is fabricated at KEK

## Slide 19: Hf-STJ development
We succeeded in observation of Josephson current by Hf-HfOx-Hf barrier layer in 2010 (S.H.Kim et. al, TIPP2011)
However, to use this as a detector, much improvement in leak current is required. ( is required to be at pA level or less)
B=10 Gauss
B=0 Gauss
HfOx：20Torr,1hour
anodic oxidation：45nm
Hf(350nm)
Hf(250nm)
Si wafer
A sample in 2012
200×200μm2
T=80~177mK
Ic=60μA
Ileak=50A@Vbias=10V
Rd=0.2Ω

## Slide 20: Hf-STJ Response to DC-like VIS light
20μV/DIV
50μA/DIV
Laser ON
Laser OFF
Laser pulse: 465nm, 100kHz
10uA/100kHz=6.2×108e/pulse
We observed an increase of tunnel current in Hf-STJ response to visible light
~10μA
V
I

## Slide 21: Summary
We propose an experiment to search for neutrino radiative decay in cosmic neutrino background.
Requirements for the detector is an ability of photon-by-photon energy measurement with better than 2% energy resolution for meV ()
Nb/Al-STJ array with grating and Hf-STJ are considered for the experiments and under development.
  Nb/Al-STJ fabricated at CRAVITY almost meets our requirement.
  FD-SOI readout for STJ signal is promising and under development.
  Hf-STJ development is in progress, but need much improvement.
It is possible to improve the neutrino lifetime lower limit up to O(1014yrs) for 200-sec measurement in a rocket experiment with the detector.

## Slide 22: Backup

## Slide 23: Energy/Wavelength/Frequency

## Slide 24: STJ I-V curve
Sketch of a current-voltage (I-V) curve for STJ
The Cooper pair tunneling current (DC Josephson current) is seen at V = 0, and the quasi-particle tunneling current is seen for |V|>2
Josephson current is suppressed by magnetic field
Leak current
B field

## Slide 25: STJ back-tunneling effect
Photon
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb/Al-STJ Nb(200nm)/Al(10nm)/AlOx/Al(10nm)/Nb(100nm)
Gain: 2～200
Nb
Al
Nb
Al