## Slide 1: Development of Superconducting Tunnel Junction Photon Detectors with Cryogenic Preamplifier for COBAND Experiment
TIPP2017 May 21-26, 2017
at Beijing International Convention Center
Shin-Hong Kim (University of Tsukuba/CiRfSE)
for COBAND Collaboration
  ● Introduction
  Motivation
  COsmic BAckground Neutrino Decay search (COBAND) experiment
  ● R&D of Superconducting Tunnel Junction (STJ) Detector
COBAND Collaboration
S.H. Kim, Y. Takeuchi, K. Takemasa, K. Nagata, K. Kasahara, S. Yagi, R. Wakasa, R. Senzaki,
K. Moriuchi, C. Asano (University of Tsukuba), S. Matsuura (Kwansei Gakuin University),
H. Ikeda, T. Wada, K. Nagase, S.Baba (JAXA), Y. Arai, I. Kurachi, M. Hazumi (KEK),
T. Yoshida, M. Sakai, T. Nakamura (University of Fukui), Y. Kato (Kindai University), K. Kiuchi,
S. Mima (RIKEN), H. Ishino, H. Kibayashi (Okayama University), S. Shiki, G. Fujii, M. Ukibe,
M. Ohkubo (AIST), S. Kawahito (Shizuoka University), E. Ramberg, M. Kozlovsky, P. Ruvinov,
D. Sergatskov (Fermilab), S.B. Kim (Seoul National University)

## Slide 2: Motivation of Search for Cosmic Background Neutrino Decay
As the neutrino lifetime is very long, we need use cosmic background neutrino to observe the neutrino decay. To observe this decay of the cosmic background neutrino means a discovery of the cosmic background neutrino predicted by cosmology.
Left-Right symmetric model predicts the neutrino lifetime larger than 1017 year while the standard model predicts 2 x 1043 year.
Measured neutrino lifetime limit τ > 3 x 1012 year.
Only neutrino mass is unknown in elementary particles. Detection of neutrino decay enables us to measure an independent quantity of Dm2 measured by neutrino oscillation experiments. Thus we can obtain neutrino mass itself
from these two independent measurements.

## Slide 3: Big-Bang Cosmology and Cosmic Background Neutrino (CνB)
A few seconds after Big Bang → Cosmic Background Neutrino (CνB)
became free.
300,000 years after Big Bang → Cosmic Microwave Background (CMB)
became free.

## Slide 4: Signal of Cosmic Background Neutrino Decay and its Backgrounds
CMB
Zodiacal Emission
Zodiacal Light
Interstellar Dust
SL
DGL
wavelength [m]
E [meV]
Surface brightness I [MJy/sr]
AKARI
COBE
Integrated flux from galaxy counts
Galaxy evolution model
CIB measurements
( AKARI,
 COBE)
By measuring the energy spectrum of the Zodiacal Emission with the CνB decay continuously, we can see the CνB decay signal as a high energy cutoff.
Rocket experiment coverage (λ＝40～80μm)
High Energy Cutoff (25meV)

## Slide 5: COBAND (COsmic BAckground Neutrino Decay Search) Experiment
JAXA Rocket CIB Experiment
（Feb 2, 1992）
  Satellite experiment after 2020 → sensitivity of τ(ν3) ~1017year
  STJ using Hafnium: Hf-STJ for satellite experiment ( S. H. Kim et al. JPSJ 81,024101 (2012)）
    : Superconducting gap energy for Hafnium
    for 25meV photon: if Fano-factor is less than 0.3
Rocket Experiment Plan: 5minutes data acquisition at 200 km height in 2019.
Improve the current limit of lifetime τ(ν3) by two orders of magnitude ( ~1014years).
Superconducting Tunneling Junction (STJ) detectors in development
  Array of 50 Nb/Al-STJ pixels with diffractive grating covering
3He sorption 0.4K
FOV = 0.006°ｘ 0.05°

## Slide 6: STJ (Superconducting Tunnel Junction）Detector
At the superconducting junction, quasi-particles over their energy gap go through tunnel barrier by a tunnel effect. By measuring the tunnel current of quasi-particles excited by an incident particle, we measure the energy of the particle.
Superconductor / Insulator / Superconductor Josephson Junction
S
I
S
2Δ
Quasi-particles
Incident Particle
Cooper Pairs
current-voltage (I-V) curve for STJ
Leakage current
( Dynamic resistance Rd in |V| < 2Δ/e)
Josephson Current
Critical current Ic
Energy gap Δ

## Slide 7: Nb/Al-STJ Photon Detector
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb(200nm)/Al(70nm)/AlOx/Al(70nm)/Nb(100nm)
  Nb/Al = 0.57meV
Gain: 2～200 (10 for Al)
Number of Quasi-particles in Nb/Al-STJ
GAl : Trapping Gain in Al(~10)
E0 : Photon Energy
Δ : E-Gap in superconductor
For 25meV single photon
Nq = 10
= 250 e
300nm
Back tunneling Effect → Trapping Gain
Response of Nb/Al-STJ to visible laser light pulse
(λ=465nm) at 350mK

## Slide 8: Leakage Current of Nb/Al-STJ
Temperature Dependence of Leakage Current
  Leakage current Ileak is required to be below 0.1nA to detect a single far-infrared photon (λ= 40 -80μm) .
  In 2014,
  AIST group joined us and produced Nb/Al-STJ with AIST CRAVITY processing system.
  Leakage current has satisfied our requirement of 0.1nA .
Ileak = 0.2nA
at 300μV
below 400mK
50μm x 50μm
by T. Fujii (AIST)
STJ size | # of samples | Ileak at 0.3mV
50 x 50μm2 | 18 | 224±29 pA
20 x 20 μm2 | 7 | 39±13 pA
10 x 10 μm2 | 20 | 14±7 pA
Ileak∝

## Slide 9
R&D of SOI-STJ Detector
To improve the signal-to-noise ratio and to make multi-pixel device easily, we made a SOI-STJ detector where we processed Nb/Al-STJ on a SOI transistor board.
    FD-SOI (Fully Depleted Silicon-On-Insulator) device was proved to operate at 4K by a JAXA/KEK group (AIPC 1185,286-289(200 FD-SOI 9)). It has the following characteristics:
    low-power consumption, high speed, easy large scale integration and suppression of charge-up by high mobility carrier due to thin depletion layer(～50nm).
    FD-SOI -MOSFET
    ～50nm
    Nb/Al-STJ
    SOI preamplifier

## Slide 10
Performance of STJ and SOIFET in SOI-STJ detector
r0
500uV /DIV.
1μs /DIV.
Signal
(1.5μs)
We observed the signal of Nb/Al-STJ processed on the SOI board to 465nm laser pulse at 700mK.
We confirmed that the SOI-FET work as a preamplifier with a gain of 8.7 at 4K up to 100kHz.
Set GAIN 8.7 @ LHe temp.

## Slide 11
SOI Cryogenic Amplifier
Amplification
Replace the resistance by a SOIFET as a current source (M2).
Feedback
Use the feedback between the drain and the gate of M1 to apply a stable bias voltage (M3).
Buffer
Add the follower to reduce the output impedance (M4 and M5).
Designed the ratio (W/L) to set the
operation power consumption below 120μW.
This SOI amplifier board was made by LAPIS semiconductor company.
SOI-STJ4 (the 4th prototype)
Vb
Vss1
V5
Vss2
Vdd1
Vdd2
V2
V3
INPUT
OUTPUT
We updated the SOI cryogenic Amplifier for Nb/Al-STJ.

## Slide 12
Test Results of the SOI Cryogenic Amplifier
Gain vs. Frequency
at 300mK
Amplifier + Buffer
Input and Amplified Output
Amplified Output (50mV/div)
Input (1mV/div)
Input
Output
Time scale 2ms/div
Gain of 80 was achieved for a signal frequency
up to 400kHz signals at 300mK.
400kHz

## Slide 13: Setup of STJ Signal Amplification with the SOI Cryogenic Amplifier
20m-square Nb/Al-STJ with SOI-STJ4 amplifier through 4.7μF capacitance.
Input impedance of the SOI amplifier is about 20kΩ.
  STJ operation at a constant current mode.
  STJ bias cable capacitance is around 1nF：Z=160Ω for 1s signal.
STJ
10M
T~350mK
(3He sorption)
465nm laser through optical fiber
GND
Vss
Vdd
4.7F
Input Monitor
Output
STJ
SOI
4.7F

## Slide 14
STJ signal amplified with the SOI cryogenic preamplifier
Temperature : 350mK
Nb/Al-STJ laser light response signal was amplified with this SOI cryogenic amplifier.
STJ signal to visible laser λ= 465nm, 20kHz
STJ amplified signal with the SOI cryogenic amplifier
Temperature : 350mK
Amplification Gain : 70
S/N improved by a factor of 2

## Slide 15
We made a thin aluminum layer (9nm) on the HfO layer (1-2 nm) to improve the insulation of the HfOX layer. Hf/Al/HfOX/Hf-STJ
Latest Results of Hf-STJ R&D
Hf
HfOX
Al(9nm)
Visible light laser (λ=465nm) 10Hz duration
Response speed (120μs) is slower than Nb/Al-STJ response speed ( around a few μs).
More details of the Hf-STJ R&D results is presented in the poster session by K. Takemasa
(P1-13).

## Slide 16: Summary
R&D of STJ detectors and the design of the COBAND rocket experiment are underway.
          Determination of the neutrino mass
                origin of elementary particle mass spectra
      Discovery of the cosmic background neutrino
            new probe of the very early universe
New far-infrared photon detector is being developed:
      Nb/Al-STJ satisfied our requirement for leakage current less than 0.1nA
      Cryogenic amplifier with the SOI technology worked at 300mK
      We have succeeded in amplifying the STJ signal with the SOI cryogenic amplifier.
      Aiming at one photon detection in the far-infrared range
      applicable to the other fields such as X-ray energy measurement with higher energy resolution.
      COBAND WEB page http://hep.px.tsukuba.ac.jp/coband/eng/

## Slide 17: BACKUP

## Slide 18: Development of SOI Charge sensitive preamplifier (SOI-STJ5)
STJ capacitance is not so small ( 20pF for 20μm square STJ).
STJ response speed is a few μsec.
STJ operation at a constant voltage mode is favorable.
  → Low input impedance
  charge amplifier
  operational for 1MHz.

## Slide 19: Op-amp Circuit for STJ (SOI-STJ5 design)
Buffer stage
Telescopic cascode
Bias
telescopic cascode differential amplifier
Feedback C=2pF x R=5MΩ = 10s
Power consumption ~150W
Iref
Iref
Iref
Iref2
10/10
W(m)/L(m)
10/10
10/10
20/10
12/7
100/7
100/7
100/1
100/1
4/1
4/1
2/10
4/10
4/10
VDD=-VSS=1.5V
Iref>10A
Iref/5
Iref2/5
Iref2/5
Test of this cryogenic charge amplifier is now underway.

## Slide 20: Neutrino Mass Relations and Expected Photon Energy Spectrum
Neutrino oscillation
ν3 → ν2 γ
Eg = 25meV
20meV
15meV
Decay Photon Energy Spectrum
Sharp edge with
1.9K smearing
Red shift effect
m3 = 50meV, m2 = 10 meV,
Eγ = 24meV

## Slide 21: Zodiacal Emission
Thermal emission from the interplanetary dust cloud
, ,
[Js], [m/s], [m]
Zodiacal Emission(ZE) is overwhelmingly dominating. Here we consider only ZE as the background.

## Slide 22: Zodiacal Emission
Surface brightness I [W/m2/sr]
1m
10m
100m
1mm

## Slide 23: Sensitivity to neutrino decay
Parameters in the rocket experiment simulation
telescope dia.: 15cm
50-column (: 40m – 80 m)  8-row array
Viewing angle per single pixel: 100rad  100rad
Measurement time: 200 sec.
Photon detection efficiency: 100%
If 3 lifetime were 2  1014 yrs, the signal significance is at 5 level
50 60 70 80
λ（μm)
Zodiacal Emission
Excess due to Neutrino Decay

## Slide 24: STJ Energy Resolution
Δ: Band gap energy
F: Fano factor (= 0.2)
E: Incident particle energy
Tc : Critical Temperature
Operation is done at a temperature around 1/10 of Tc
STJ Energy Resolution
We reported that Hf-STJ worked as a STJ in TIPP2011.
Material |  | 
Niobium | 9.20 | 1.550
Aluminum | 1.14 | 0.172
Hafnium | 0.13 | 0.021

## Slide 25: STJ back tunneling effect
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb/Al-STJ Nb(200nm)/Al(10nm)/AlOx/Al(10nm)/Nb(100nm)
Gain: 2～200
Photon
Nb
Al
Nb
Al

## Slide 26
Performance of SOIFET at Cryogenic Temperature
Saturating current is higher as the temperature becomes lower.
Non-linearity was found at cryogenic temperature near threshold region. This problem was solved by improving LDD(Lightly Doped Drain).
At cryogenic temperature (3K),
Threshold rise in Ids-Vds curve become much sharper.
Subthreshold current is suppressed.
̶̶ ROOM
̶̶̶ 3K
Vds (V)
Ids (A)
Vgs (V)
Ids (A)
̶̶ ROOM
̶̶̶ 3K

## Slide 27
Test Results of the cryogenic SOI preamplifier
Amplifier gains are around 50 both at room temperature and 3K with adjusted bias voltages of M2.
Bandwidth of buffer is enough high for the amplifier of STJ signal (up to 200kHz) both at room temperature and 3K.
Amplifier
Buffer

## Slide 28
Temperature Dependence of I-V curve
Threshold voltage is changed. But the other properties are almost unchanged.

## Slide 29: Test Results of Nb/Al-STJ with Far-Infrared laser
Nb/Al-STJ Response to Far-Infrared Laser
20m-square Nb/Al-STJ made at AIST CRAVITY system
Laser light was turned on and off with a chopper at a frequency of 200Hz. Measured the change of the I-V curve between the laser on and off to be 50~100nA in current.
Far-Infrared Laser at University of Fukui（=57.2m）