## Slide 1: Development of Superconducting Tunnel Junction Photon Detectors for Cosmic Background Neutrino Decay Search
IWSSD2014 November 8, 2014
Shin-Hong Kim (University of Tsukuba)
for Neutrino Decay collaboration
  ● Introduction
  Motivation
  Proposal on Search for Cosmic Background Neutrino Decay
  Preparatory Rocket experiment
  ● R&D of Superconducting Tunnel Junction (STJ) Detector
Neutrino Decay Collaboration
S.H. Kim, Y. Takeuchi, K. Takemasa, K. Kiuchi, K. Nagata, K. Kasahara, T. Okudaira, T. Ichimura,
M. Kanamaru, K.Moriuchi, R. Senzaki (University of Tsukuba), H. Ikeda, S. Matsuura, T. Wada,
(JAXA/ISAS), H. Ishino, H. Kibayashi (Okayama University), S. Mima (RIKEN), T. Yoshida,
K. Orikasa, R. Hirose (University of Fukui), Y. Kato (Kinki University), M. Hazumi, Y. Arai (KEK),
E. Ramberg, J.H. Yoo, M. Kozlovsky, P. Ruvinov, D. Sergatskov (Fermilab),
S.B. Kim (Seoul National University)

## Slide 2: Motivation of Search for Cosmic Background Neutrino Decay
As the neutrino lifetime is very long, we need use cosmic background neutrino to observe the neutrino decay. To observe this decay of the cosmic background neutrino means a discovery of the cosmic background neutrino predicted by cosmology.
Left-Right symmetric model predicts the neutrino lifetime larger than 1017 year while the standard model predicts 2 x 1043 year.
Measured neutrino lifetime limit τ > 3 x 1012 year.
Only neutrino mass is unknown in elementary particles. Detection of neutrino decay enables us to measure an independent quantity of Dm2 measured by neutrino oscillation experiments. Thus we can obtain neutrino mass itself
from these two independent measurements.

## Slide 3: Big-Bang Cosmology and Cosmic Background Neutrino (CnB)

## Slide 4: Signal of Cosmic Background Neutrino Decay and its Backgrounds
CMB
Zodiacal Emission
Zodiacal Light
Interstellar Dust
SL
DGL
wavelength [m]
E [meV]
Surface brightness I [MJy/sr]
AKARI
COBE
Integrated flux from galaxy counts
Galaxy evolution model
CIB measurements
( AKARI,
 COBE)
By measuring the energy spectrum of the Zodiacal Emission with the CνB decay continuously, we can see the CνB decay signal as a high energy cutoff.
Rocket experiment coverage (λ＝40～80μm)
High Energy Cutoff (25meV)

## Slide 5: JAXA Rocket Experiment for Neutrino Decay Search
JAXA Rocket CIB Experiment
（Feb 2, 1992）
  Satellite experiment after 2020 → sensitivity of τ(ν3) ~1017year
  STJ using Hafnium: Hf-STJ for satellite experiment ( S. H. Kim et al. JPSJ 81,024101 (2012)）
    : Superconducting gap energy for Hafnium
    for 25meV photon: if Fano-factor is less than 0.3
Plan: 5minutes data acquisition at 200 km height in 2017 in earliest.
Improve the current limit of lifetime τ(ν3) by two orders of magnitude ( ~1014years).
Superconducting Tunneling Junction (STJ) detectors in development
  Array of 50 Nb/Al-STJ pixels with diffraction grating covering

## Slide 6: STJ (Superconducting Tunnel Junction）Detector
At the superconducting junction, quasi-particles over their energy gap go through tunnel barrier by a tunnel effect. By measuring the tunnel current of quasi-particles excited by an incident particle, we measure the energy of the particle.
Superconductor / Insulator / Superconductor Josephson Junction
S
I
S
2Δ
Quasi-particles
Incident Particle
Cooper Pairs
current-voltage (I-V) curve for STJ
Leakage current
( Dynamic resistance Rd in |V| < 2Δ/e)
Josephson Current
Critical current Ic
Energy gap Δ

## Slide 7: Nb/Al-STJ Photon Detector
 | Si | Nb | Al
Tc[K] |  | 9.23 | 1.20
Δ[meV] | 1100 | 1.550 | 0.172
Number of Quasi-particles in Nb/Al-STJ
GAl : Trapping Gain In Al(~10)
E0 : Photon Energy
Δ : E-Gap in superconductor
For 25meV single photon
Nq = 10
= 95 e
300nm
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb/Al-STJ Nb(200nm)/Al(10nm)/AlOx/Al(10nm)/Nb(100nm)
Gain: 2～200
Back tunneling Effect → Trapping Gain

## Slide 8
R&D of Superconducting Tunnel Junction (STJ) Detctor
Nb/Al-STJ
Goal: detection of a single far-infrared photon in the energy range of 15 – 30 meV (λ= 40 -80μm) for the rocket experiment for neutrino decay search.
Signal charge
distribution
Signal of Nb/Al-STJ (100 x 100μm2) to
infrared (1.31μm) light at 1.9K.
Time spread at FWHM is 1μsec.
The number of photon : 93±11
( from the spread of
the signal charge distribution ).
the response of Nb/Al-STJ (4μm2 ) to the visible light (465nm) at 1.9K.
a single photon peak is separated from pedestal by 1σ.
The signal charge distribution (Red histogram) is fitted by four Gaussians of 0, 1, 2 and 3 photon peaks. Single photon peak has a mean of 0.4fC and σ of 0.4fC.

## Slide 9: Requirement for the cold amplifier of STJ readout
● Response speed
  The integration time of charge is 2-4μs.
● Low power consumption
  Typical cooling power of our refrigerator is 400μW.
1. Operation below 800mK
2. Power consumption of the amplifier should be as low as possible.
3. Amplification gain should be large enough up to 1MHz.
Temperature Dependence of Leakage Current with Nb/Al-STJ(100x100μm2 )
3He sorption refrigerator is our candidate
To 100pA
100pA@800mK
  We need the preamplifier operated at extremely low temperature to detect a single far-infrared photon (λ= 40 -80μm) .
● Operation at ultra-low temperature
  Requirement for leakage current of Nb/Al-STJ is below 100pA.
  We reduce it by using smaller one.
  Thermal excitation()
  We need to make cooler 800mK.

## Slide 10
R&D of SOI-STJ Detctor
To improve the signal-to-noise ratio and to make multi-pixel device easily, we made a SOI-STJ detector where we processed Nb/Al-STJ on a SOI transistor board.
We confirmed that both Nb/Al-STJ detector and SOI MOSFET worked normally at 750mK.
    FD-SOI (Silicon-On-Insulator) device was proved to operate at 4K by a JAXA/KEK group (AIPC 1185,286-289(200 FD-SOI 9)). It has the following characteristics:
    low-power consumption, high speed, easy large scale integration and suppression of charge-up by high mobility carrier due to thin depletion layer(～50nm).
    FD-SOI -MOSFET
    ～50nm

## Slide 11: Performance of Nb/Al-STJ in SOI-STJ Detector
2 mV /DIV.
1 mA /DIV.
500μV /DIV.
10 nA /DIV.
2mV /DIV.
50μA /DIV.
2 mV /DIV.
1 mA /DIV.
Ic～200μA
Ｅｎｌａｒｇｅｄ
We measured the I-V curve of the Nb/Al-STJ (50 x 50μm2 junction) processed on the SOI wafer
at 700mK with a dilution refrigerator.
I-V curve of Josephson Junction
Leak current @ 0.5mV is 6nA. It is close to our best record of normal Nb/Al-STJ(100um x 100um) 10nA.
Quality Factor (Rdynamic/Rnormal)
On Si wafer : 5 x 105
On SOI wafer : 3 x 105
B=35 G
Ｅｎｌａｒｇｅｄ
Signal of Nb/Al-STJ in SOI-STJ for 465nm laser pulse.

## Slide 12
Performance of SOIFET in SOI-STJ detector
● Temperature dependence
I-V curves at various temperatures.
SOIFET can be operated at 100mK.
● Power consumption ( at 680mK )
Bias voltage of SOIFET in saturation
region (red line) : 0.5 V
Current (Ids)of FET in saturation region
at Vgs = 0.8V : 0.09 μA
Power consumption = 0.5 V ×0.09 μA
= 45 nW/FET
for W/L=1.42μm/0.42μm

## Slide 13
Future Plan of SOI-STJ R&D
We are updating the SOI-STJ design for the amplification of the Nb/Al-STJ signal.
  Replace the resistance to SOIFET that we use as a current source.
  Use the feedback between the drain and the gate to apply a stable bias voltage
  Add the follower to reduce the output impedance.
Designed the ratio (W/L) to set the operation power consumption below 120μW.
AIST group joined us on the SOI-STJ R&D and is processing the STJ on the SOI board made by LAPIS.
We will measure the response of this new SOI-STJ to laser light soon.

## Slide 14
R&D of Superconducting Tunnel Junction (STJ) Detctor
Hf-STJ
Goal: Measure energy of a single far-infrared photon for neutrino decay search experiment within 2% energy resolution.
Hf-STJ (100x100mm2) shows smaller leakage current than Hf-STJ (200x200mm2) which we have established to work as a STJ in 2011.
The work to reduce a large leakage current of
Hf-STJ is underway.
B=10 Gauss
B=0 Gauss
I-V curve of Hf-STJ (200x200m2 )
T~80mK, Ic=60μA, Rd=0.2Ω
I-V curve of Hf-STJ (100x100m2 )
T~40mK, Ic=10μA, Rd=0.6Ω
B=0 Gauss
B=10 Gauss

## Slide 15
V : 20μV/div
Red；with light
Yellow：without light
Hf-STJ Response to DC visible light
I-V Curve with and without
visible laser light (λ=465nm f=100kHz)
100×100μm2
T=39~53mK
Rd=0.6Ω
Hf(350nm)
Hf(250nm)
Si wafer
HfOx：20Torr,1hour 1.5nm
I: 50μA/div
ΔI =10μA
at 20 μV
We are testing smaller Hf-STJ’s to decrease the leakage current.

## Slide 16: Summary
We are developing STJ-based detectors to detect a single far-infrared photon in energy range between 15 and 30meV to search for the cosmic background neutrino decay with a rocket or satellite experiment.
The SOI-STJ detector where Nb/Al-STJ’s were processed on a SOIFET board is being developed. Both SOIFET and STJ are working well in the SOI-STJ detector below 800mK.
Hf-STJ response to the visible light was observed. Improvement to reduce the leakage current is underway.

## Slide 17: BACKUP

## Slide 18: Schedule
18
18
Nb/Al-STJ設計・開発
 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019
Experiment Design |  |  |  |  |  | 
SuperconductingTunnel Junction (STJ ) Detector |  |  |  |  |  | 
Preamplifier at 2K and Post-Preamp (Fermilab, JAXA, KEK, AIST, Tsukuba） |  |  |  |  |  | 
Dispersive Element, Optics (JAXA, Tsukuba) |  |  |  |  |  | 
Cryostat ( JAXA, KEK) |  |  |  |  |  | 
Measurements＋Analysis （All） |  |  |  |  |  | 
Experiment design with FIR Rocket
Experiment design with Satellite such as SPICA
Design and R&D of Nb/Al-STJ Detector
Production
Production
Design and R&D
Simulation
Design and R&D
Design and R&D of Hf-STJ Detector
Production
Analysis Program
Analysis
Design and R&D
Production
Far-Infrared Observatory Rocket Experiment

## Slide 19: Big-Bang Cosmology and Elementary Particle Physics
CDF
ATLAS
GUT
Phase Transition in vacuum
Electroweak
Higgs particle
1.9K Cosmic background neutrino
(110/cm3)
2.7K Cosmic background
radiation(420/cm3)

## Slide 20: Neutrino Lifetime
WL and WR are fields with pure V-A and V+A couplings, respectively, and z is a mixing angle.
Measured neutrino lifetime limit τ < 3 x 1012 year
from CIB results measured by COBE and AKARI

## Slide 21: Neutrino Mass Relations and Expected Photon Energy Spectrum
Neutrino oscillation
ν3 → ν2 γ
Eg = 25meV
20meV
15meV
Decay Photon Energy Spectrum
Sharp edge with
1.9K smearing
Red shift effect
m3 = 50meV, m2 = 10 meV,
Eγ = 24meV

## Slide 22: Neutrino Decay Detection Sensitivity
10-hour running with
a telescope with 20cm diameter,
a viewing angle of 0.1 degrees
and 100% detection efficiency
( Satellite Experiment )
dN/dEγ
- d2Nγ/dEγ2
● Need the energy resolution better
than 2%.
● Can observe the ν3 decay with
a mass of 50meV, and a lifetime of
1.5 x 1017year at 6.7σ.
Cosmic Infrared Background
Neutrino Decay （τ＝1.5 x 1017year）
Sharp edge with 1.9K smearing
with detector resolution of 0% to 5%
6.7σ
Red shift effect

## Slide 23: 5σ observation sensitivity by 10-hour measurement with a telescope with 20 cm diameter, a viewing angle of 0.1 degree
SU(2)L x SU(2)R x U(1) model Lifetime Prediction
Search Region: λ＝ 40～150μm （Eγ ＝ 8～30meV）
In Rocket experiment, λ＝ 40～80μm （Eγ ＝ 15～30meV）
Nb/Al-STJ sensisitive region > 8meV ( Nquasi-particles = 60 )
S.H. Kim, K. Takemasa, Y. Takeuchi and S. Matsuura JPSJ 81, 024101 (2012)
Search Region ( Satellite Experiment)
Rocket Experiment

## Slide 24: Lifetime Calculation
R. E. Schrock, Nucl. Phys. 28 (1982) 359.
Calculate the neutrino decay width in SU(2)L ｘ SU(2)R ｘ U(1) model

## Slide 25: STJ Energy Resolution
Δ: Band gap energy
F: Fano factor (= 0.2)
E: Incident particle energy
Tc : Critical Temperature
Operation is done at a temperature around 1/10 of Tc
STJ Energy Resolution
We reported that Hf-STJ worked as a STJ in 2011.
Material |  | 
Niobium | 9.20 | 1.550
Aluminum | 1.14 | 0.172
Hafnium | 0.13 | 0.021

## Slide 26: STJ back tunneling effect
Photon
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb/Al-STJ Nb(200nm)/Al(10nm)/AlOx/Al(10nm)/Nb(100nm)
Gain: 2～200
Nb
Al
Nb
Al

## Slide 27: JAXA Rocket Experiment for Neutrino Decay Search
Focal plane Instruments
Incident rays are made parallel through cylindrical mirrors 1, 2 and a parabolic mirror before diffracted by a grating, and are finally focused on the STJ detector array by a spherical mirror.
Rate/50pixel-spectrometer = 15 kHz ( 300Hz/pixel)
Measurements for 200 s → 3M events /50pixel-spectrometer.
Using 8 x 50pixel-spectrometer, σ/N=0.02%
2σ = 0.04% x 0.5μW/m2/sr = 0.2nW/m2/sr (0.4% times present limit 50nW/m2/sr ）

## Slide 28: Cosmic Infrared Background measured by COBE and AKARI
COBE: M. G. Hauser et al. ApJ 508 (1998) 25. D. P. Finkbeiner et al. ApJ 544 (2000) 81.
AKARI: S. Matsuura et al. ApJ. 737 (2011) 2.
A. Mirizzi, D. Montanino and P. Serpico PRD76, 053007 (2007)
Neutrino lifetime τ < (1.6~3.1)x1012 year from CIB results by COBE
S.H. Kim, K. Takemasa, Y. Takeuchi and S. Matsuura JPSJ 81, 024101 (2012)
Neutrino lifetime τ < (3.1~3.8)x1012 year from CIB results by AKARI and SPITZER
Zodiacal Light
Surface brightness lIl
Galactic dust emission
Wavelength[m]
Integrated flux from galaxy counts
Galaxy evolution model
CIB measurements
( AKARI,  COBE)
Search Region
Rocket Experiment

## Slide 29: Expected Photon rate per 1pixel
Telescope
  Zodiacal emission 343Hz / pixel
  200sec measurement: 0.55M events / 8 pixels (at )
  0.13% accuracy measurement for each wavelength
  =0.6nW/m2/sr
Neutrino decay (yr)
  =1.5nW/m2/sr
  2.3σ away from fluctuation in zodiacal emission measurement
Zodiacal Light
Zodiacal Emission
Galaxy evolution model
Galactic dust emission
Integrated flux from galaxy counts
CMB
yr
 with yr is possible to detect!

## Slide 30: Signal of Cosmic Background Neutrino Decay and its Backgrounds
CMB
Zodiacal Emission
Zodiacal Light
Interstellar Dust
SL
DGL
wavelength [m]
E [meV]
Surface brightness I [MJy/sr]
AKARI
COBE
Integrated flux from galaxy counts
Galaxy evolution model
CIB measurements
( AKARI,
 COBE)
60-days running with a telescope with 20cm diameter, a viewing angle of 0.1°and 100% detection efficiency ( Satellite Experiment ) sensitivity τ < 1017 year.
5-minutes running with a telescope in rocket experiment (preparatory experiment) sensitivity τ < 1014 year ( two-order improvement).
By measuring the energy spectrum of the Zodiacal Emission with the CνB decay continuously, we can see the CνB decay signal as a high energy cutoff.
Rocket experiment coverage (λ＝40～80μm)
High Energy Cutoff (24meV)

## Slide 31: Feasibility of FIR single photon detection
Assume typical time constant from STJ response to pulsed light is ~1μs
Assume leak current is 0.1nA
Fluctuation due to electron statistics in 1μs is
While expected signal charge for 25meV are
(Assume back tunneling gain x10)
  More than 3sigma away from leakage fluctuation
Requirement for amplifier
    Noise<16e
    Gain: 1V/fC  V=16mV

## Slide 32
Performance of SOIFET in SOI-STJ detector
r0
500uV /DIV.
1μs /DIV.
Signal
(1.5μs)
We observed the signal of Nb/Al-STJ processed on the SOI board to 465nm laser pulse.
The width of the signal of Nb/Al-STJ is about 1μs.
Our requirement for the cold preamplifier is to operate at 1 MHz to have the best siganl-to-noise ratio.
We confirmed that the SOI-FET as the preamplifier with a gain of 8.7 at 4K up to 100kHz.
Set GAIN 8.7 @ LHe temp.

## Slide 33
Performance of SOIFET in SOI-STJ detector
NMOS(690-750mK)
Width = 1000μm
Length = 1μm
PMOS(750mK)
Width = 1000μm
Length = 1μm
NMOS
PMOS
I-V curve of SOIFETs after processing Nb/Al-STJ.
Both of NMOS and PMOS could be operated below 800mK.
Transconductance “gm” did not vary drastically as a function of temperature at the operation voltage of 0.2V.
  We can use these as Preamplifier for STJ signal
at ultra-low temperature.
Ids [A]
-Ids [A]
Vgs[V]
Vgs[V]
gm [S]
gm [S]
Vds[V]
Vds[V]

## Slide 34
Temperature Dependence of I-V curve
Threshold voltage is changed. But the other properties are almost unchanged.