## Slide 1: 超伝導体検出器 ― SOI技術との融合による遠赤外一光子検出 STJ 開発 ―
2015年11月30日 /光量子計測器開発推進室発足会議
武内勇司 (筑波大 数理物質融合科学センター)
on behalf of Neutrino Decay Collaboration
S. H. Kim, K. Takemasa, K. Kiuchi, K. Nagata, K. Kasahara, K. Moriuchi, R. Senzaki, S. Murakami, S. Yagi (U. Tsukuba), S. Matsuura (Kwansei Gakuin U.), H. Ikeda, T. Wada, K. Nagase (JAXA/ISAS), H. Ishino, A. Kibayashi (Okayama U.), S. Mima (RIKEN), T. Yoshida, R. Hirose, Y. Kato, C. Asano, T. Nakamura (U. Fukui), Y. Kato (Kinki U.), Y. Arai, M. Hazumi, I. Kurachi (KEK), S. Shiki, M. Ukibe, G. Fujii, M. Ohkubo (AIST), E. Ramberg, J. H. Yoo, M. Kozlovsky, P. Rubinov, D. Sergatskov (FNAL), S. B. Kim (Seoul National U.) and S. Kawahito (Shizuoka U.)

## Slide 2: Superconducting Tunnel Junction (STJ)
接合面を挟んで電位差(|V|<2)を印加.
超伝導体に吸収された光子のエネルギーにより複数のクーパー対が解離(励起)し，生成された準粒子によって，エネルギーに比例したトンネル電流が発生．
Superconductor / Insulator /Superconductor Josephson junction device
Δ: Superconducting gap energy
2
E
Ns(E)
Superconductor
Superconductor
Insulator
Insulator
Superconductor
100m
300nm
超伝導ギャップ(Δ)は遠赤外フォトンのエネルギーよりもずっと小さい  原理的には，遠赤外域一光子を検出可能
~s 程度の比較的高速なパルス応答(Nbの場合)  光子計数することでS/Nの著しい向上

## Slide 3: STJ I-V 特性
Sketch of a current-voltage (I-V) curve for STJ
The Cooper pair tunneling current (DC Josephson current) is seen at V = 0, and the quasi-particle tunneling current is seen for |V|>2
Josephson current is suppressed by magnetic field
Leak current
B field
光入射の場合

## Slide 4: 宇宙背景ニュートリノ崩壊探索への応用
 distribution in
Two body decay
dN/d(a.u.)
[m]
100
500
10
Red Shift effect
Sharp Edge with 1.9K smearing
in the 3 rest frame
Nb/Al-STJ array
8 rows
50 columns

## Slide 5: 宇宙背景ニュートリノ崩壊探索への応用
Telescope parameters
Main mirror
  D=15cm, F=1m
detector
  波長0.8m あたり
  100m x 100m x 8 pixels
  視野角 : 8 x 10-8 sr
CMB
ISD
SL
DGL
CB decay
wavelength [m]
Surface brightness I [MJy/sr]
Zodiacal Emission
Zodiacal Light
Integrated flux from galaxy counts
Neutrino decay (, yrs): =25kJy/sr
  3.3 x 10-20 W / 8pixels @ =50m
200sec の測定でこれを検出
 検出器の性能として最低でも NEP < が必要
  実際には，本物のフォトンによるバックグラウンド(Zodiacal emission)があるので，更に1 order 位低い必要がある (NEP<)

## Slide 6: 産総研 CRAVITY 製 Nb/Al-STJ
Temperature(K)
0.3
0.4
0.5
0.6
0.7
Leakage
100pA
1nA
10nA
100nA
50m  50m Nb/Al-STJ fabricated in CRAVITY at AIST
Ileak~0.2nA を達成
更に小さな junction size のものでテスト中
0.1nA
M. Ukibe et al., Jpn. J. Appl. Phys. 51, 010115 (2012)
M. Ohkubo et al., IEEE Trans. Appl. Super, 24, 2400208 (2014)
リーク電流のショットノイズ由来のNEPは，リーク電流iL=50pA, 超伝導ギャップエネルギー=0.6meV, トラッピングゲインG=10とすると
500pA/DIV
0.2mV/DIV
I
V
T~0.3K
w/ B field

## Slide 7: STJパルス光応答特性
100uV/div
4us/div
T.Okudaira，2015.1.16
可視光(465nm)レーザーパルス応答性(AIST製Nb/Al-STJ 100um角)
STJ 応答信号時定数: 立下り ~1s, 立上り~2s
(もしくは，これより早い)
VIS laser through optical fiber
STJ
V
冷凍機
V0
R0=1M
I
V
STJ I-V curve w/light w/o light
V0=V+R0I
0.4mV
定電流モードの回路(右上)で測定
Nb/Al-STJは，~1s という比較的早い応答速度
光子計数を行えば，実効的なNEPは劇的に改善可能
  但し読出し系の帯域は>1MHzを確保する必要あり

## Slide 8: STJ キャパシタンス測定
STJ
I=I(V)
CSTJ
Current (nA)
Voltage (mV)
0
0.4
-0.4
0
40
-40
緑：実測 (f=2kHz)
黒：シミュレーション
CSTJ=0.9nF, 1.2nF,1.5nF, 1.8nF
STJ は，junction size に比例したキャパシタンス
STJのI-V測定からSTJのキャパシタンスを測定
SIS接合面の面積に比例する成分： ~34fF/m2
20m角のSTJでも 14pF
低入力インピーダンスの電荷積分型アンプでの読出しが必要
STJ 等価回路
100mx100m

## Slide 9: 100x100m2 Nb/Al-STJ response to 465nm multi-photons
Laser pulse trigger
2V/DIV
40μs/DIV
産総研CRAVITY製100x100m2 Nb/Al-STJ
Pulse height dispersion is consistent with 10-photon detection in STJ
STJ
T~350m
(3He sorption)
Charge sensitive +
pre-amp.
CSTJ
10M
Shaper
amp.
I=I(V)
Nb/Al-STJ の低入力インピーダンス電荷積分アンプ読出
可視光パルス（波長465nm）に対する応答
室温に置かれた電荷積分型のアンプでの読出
  観測した出力電荷量は，およそ10光子の検出に対応
一光子検出には，読み出し系のS/N改善が必要
  極低温電荷積分型アンプの開発

## Slide 10: Development of SOI-STJ
SOI: Silicon-on-insulator
  CMOS in FD-SOI is reported to work at 4K by T. Wada (JAXA), et al.
SOI と STJ の融合 (SOI回路一体型 STJ の基礎研究)
  STJ layers are fabricated directly on a SOI pre-amplifier board and cooled down together with the STJ
Started test with Nb/Al-STJ on SOI with p-MOS and n-MOS FET
SOI
STJ
Nb
metal pad
STJ lower layer has electrical contact with SOI circuit through VIA
J Low Temp Phys 167, 602 (2012)
VIA
STJ
capacitor
FET
700 um
640 um
C
SOI-STJ2 circuit
D
S
G

## Slide 11: SOI上にSTJを形成後の特性
Both nMOS and pMOS-FET in FD-SOI wafer on which a STJ is fabricated work fine at temperature down below 1K
  極低温では，スレッショルド電圧のシフト，サブスレッショルド領域のドレイン電流抑制，飽和領域でのドレイン電流の上昇など，特性が変動
Nb/Al-STJ fabricated at KEK on FD-SOI works fine
We are also developing SOI-STJ where STJ is fabricated at CRAVITY
B~150Gauss
2mV/DIV
1mA/DIV
I-V curve of a STJ fabricated at KEK on a FD-SOI wafer
nMOS-FET in FD-SOI wafer on which a STJ is fabricated at KEK
gate-source voltage (V)
drain-source current
0
0.2
0.4
0.6
0.8
-0.2
1pA
1nA
1A
1mA

## Slide 12: SOI Pre-amplifier development
STJ に定バイアスを印加するのと同時にSTJに発生した電荷を積分
遠赤外一光子検出に向け，前段階として近赤外一光子検出に最適化した電荷積分型アンプをVDEC* が提供するSPICE simulation で設計中
極低温での SOI MOSFET の振る舞いをシミュレーションに組み込むため KEK や JAXA と共同研究で SPICE用MOSFETパラメータを構築中
  様々なL(チャンネル長：L=0.4~5um)やW(チャンネル幅: W=1~10um)を持ったFETの3Kにおける特性の測定
* VLSI Design and Education Center(VDEC), the U. Tokyo in collaboration with Synopsys, Inc., Cadence Design Systems, Inc., and Mentor Graphics, Inc.
-
+
V=0.4mV
Output
STJ
I=I(V)
CSTJ
500M
1pF
50s
0s
100s
室温でのFET パラメータを仮定したSPICE simulation
入力電荷:2fC
1.3eV(波長1m)の一光子入射相当

## Slide 13: まとめ
遠赤外(50m)の一光子検出が可能な検出器を STJ + SOI の技術を用いて開発中
  光子計数により，実効的にNEP で を目指す
Nb/Al-STJ は，産総研CRAVITY で世界最高水準の低リーク電流のものが得られている(<200pA @ 50m角)
  20μm角，10m角のものもテスト中
SOIに技術を用いた極低温アンプによる読出し回路を開発中
  様々なW/LをもつSOI MOSFETの極低温でのI-V測定SPICE シミュレーションにもちいるFETパラメータ抽出
  光子計数の利点を最大限に生かす高速アンプ(帯域>1MHz)
  SOI アンプ一体型STJの可能性

## Slide 14: Backup

## Slide 15: Neutrino
Neutrino has 3 mass generations (1, 2, 3)
Neutrino flavor states (e, , ) are not mass eigenstates
Neutrino flavor oscillates during the flight, and squared mass differences (, ) have been measured, but their absolute masses are not measured yet!
Heavier neutrinos (2, 3) are not stable
  Neutrino can decay through the loop diagrams
  Neutrino mass can be determined from the decay
However, neutrino lifetime is expected to be very long (much longer than the age of universe)
We adopt Cosmic neutrino background (CB) as the neutrino source for neutrino decay search

## Slide 16: Cosmic neutrino background (CB)
CMB
CB (=neutrino decoupling)
The universe is filled with neutrinos.
However, they have not been detected yet!
Density (cm-3)
~1s after the big bang

## Slide 17: Motivation of -decay search in CB
Search for in cosmic neutrino background (CB)
  Search for anomalous magnetic moment of neutrino
  Direct detection of CB
  Determination of neutrino mass:
Aiming at a sensitivity to lifetime for
  Standard Model expectation:
  Experimental lower limit:
  L-R symmetric model (for Dirac neutrino) predicts down to for - mixing angle
LRS: SU(2)LｘSU(2)RｘU(1)B-L
SM: SU(2)Lｘ U(1)Y
Suppressed by and GIM
Only suppressed by L-R mixing ()
1026 enhancement to SM
Magnetic moment term
(need L-R coupling)
PRL 38,(1977)1252, PRD 17(1978)1395

## Slide 18: Photon Energy (Wavelength) in Neutrino Decay
m3=50meV
m1=1meV
m2=8.7meV
E =4.4meV
E =24meV
 distribution in
E =24.8meV
Two body decay
()
()
()
From neutrino oscillation
From Planck+WP+highL+BAO
50meV<<87meV
  14~24meV (51~89m)
dN/d(a.u.)
[m]
100
500
10
Red Shift effect
Sharp Edge with 1.9K smearing
in the 3 rest frame

## Slide 19: CB decay signal and Backgrounds
at λ＝50μm
Zodiacal Emission(ZE)
~ 8 MJy/sr
CIB
~ 0.1-0.5 MJy/sr
~ 0.8MJy/sr
~ 25kJy/sr
Expected spectrum
Surface brightness I [MJy/sr]
CB decay
λ＝50 μm
E=25 meV
Excluded by S.H.Kim et. al 2012
E [meV]
wavelength [m]
CB decay
AKARI
COBE
CMB
ZE
ZL
DGL
ISD
SL
CIB summary from Matsuura et al.(2011)

## Slide 20
Proposed rocket experiment
with a diffraction grating and Nb/Al-STJ array combination
  200-sec measurement at altitude of 200~300km
    Telescope with diameter of 15cm and focal length of 1m
    All optics (mirrors, filters, shutters and grating) will be cooled at ~1.8K
  At the focal point, diffraction grating covering =40-80m (16-31meV) and array of Nb/Al-STJ pixels of 50(in wavelength distribution) x 8(in spatial distribution) are placed
  Each Nb/Al-STJ pixel is used as a single-photon counting detector for FIR photon in ()
  Sensitive area of 100mx100m for each pixel (100rad x 100rad in viewing angle)
Nb/Al-STJ array
8 rows
50 columns

## Slide 21: Expected precision in the spectrum measurement
Telescope parameters
Main mirror
  D=15cm, F=1m
detector
  sensitive area 100mx100m / pixel
  50 x 8 array
CMB
ISD
SL
DGL
CB decay
wavelength [m]
Surface brightness I [MJy/sr]
Zodiacal Emission
Zodiacal Light
  Zodiacal emission 343Hz / pixel
  200sec measurement: 0.55M events / 8 pixels (at )
  0.13% accuracy measurement for each wavelength: =11kJy/sr
Neutrino decay (, yrs): =25kJy/sr
  2.3σ away from statistical fluctuation in ZE measurement
Integrated flux from galaxy counts
 decay with yrs is possible to detect, or set lower limit!

## Slide 22: Sensitivity to neutrino decay
Parameters in the rocket experiment simulation
telescope dia.: 15cm
50-column (: 40m – 80 m)  8-row array
Viewing angle per single pixel: 100rad  100rad
Measurement time: 200 sec.
Photon detection efficiency: 100%
Can set lower limit on 3 lifetime at 4-6  1014 yrs if no neutrino decay observed
If 3 lifetime were 2  1014 yrs, the signal significance is at 5 level

## Slide 23: Energy/Wavelength/Frequency

## Slide 24: STJ back-tunneling effect
Photon
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb/Al-STJ Nb(200nm)/Al(10nm)/AlOx/Al(10nm)/Nb(100nm)
Gain: 2～200
Nb
Al
Nb
Al

## Slide 25
STJ energy resolution
Statistical fluctuation in number of quasi-particles  energy resolution
Smaller superconducting gap energy Δ yields better energy resolution
 | Si | Nb | Al | Hf
Tc[K] |  | 9.23 | 1.20 | 0.165
Δ[meV] | 1100 | 1.550 | 0.172 | 0.020
Δ: Superconducting gap energy
F: fano factor
E: Photon energy
Hf
Hf-STJ is not established as a practical photon detector yet
Nq.p.=25meV/1.7Δ=735
  2% energy resolution is achievable if Fano factor <0.3
  for a single-photon
Tc :SC critical temperature
Need ~1/10Tc for practical
operation
Nb
Well-established as Nb/Al-STJ
(back-tunneling gain from Al-layers)
Nq.p.=25meV/1.7Δ=9.5
Poor energy resolution, but a single-photon detection is possible
Notes: 25

## Slide 26: 検出器に要求されるNEP
Telescope parameters
Main mirror: D=15cm, F=1m
detector
  波長0.8m (=(80m-40m)/50, =c/50m-c/50.8m=94GHz)あたり
  100m x 100m x 8 pixels  視野角 : 8 x 10-8 sr
Neutrino decay (, yrs): =25kJy/sr @ =50m
Zodiacal emission: =8MJy/sr @ =50m
t 時間でFZE 積分した際の揺らぎ
エネルギーのフォトン数揺らぎ起因：
測定条件，検出器要件を決める不等式
 t>40sec (1), t>200sec (2.2)
 for t=200sec with 8 pix