## Slide 1: Experimental search for the cosmic background neutrino decay in the cosmic far-infrared background
TGSW 2014
Sep. 29th, 2014 / University of Tsukuba, Japan
Yuji Takeuchi (Univ. of Tsukuba)
for Neutrino Decay Collaboration
S.H.Kim , K. Takemasa, K.Kiuchi , K.Nagata , K.Kasahara , T.Okudaira, T.Ichimura, M.Kanamaru, K.Moriuchi, R.Senzaki(Univ. of Tsukuba), H.Ikeda, S.Matsuura, T.Wada(JAXA/ISAS), H.Ishino, A.Kibayashi (Okayama Univ), S.Mima (RIKEN), T.Yoshida, S.Komura, K.Orikasa, R.Hirose(Univ. of Fukui), Y.Kato(Kindai Univ.), Y.Arai, M.Hazumi(KEK), E.Ramberg, J.H.Yoo, M.Kozlovsky, P.Rubinov, D.Sergatskov(Fermilab) S.B.Kim(Seoul National Univ.)

## Slide 2: Contents
Introduction to neutrino decay search
  Proposed rocket experiment
Candidates for far-infrared single photon detector/spectrometer
  Nb/Al-STJ with diffraction grating
  Hf-STJ
Summary

## Slide 3: Neutrino
Neutrino has 3 mass generations (1, 2, 3)
Neutrino flavor states (e, , ) are not mass eigenstates
Neutrino can decay through the loop diagram
Neutrino lifetime is very long
Cosmic neutrino background (CB) is the best neutrino source for neutrino decay search

## Slide 4: Cosmic neutrino background (CB)
CMB
CB (~1s after big bang)
Not yet observed experimentally

## Slide 5: Motivation of -decay search in CB
Search for in cosmic neutrino background (CB)
  Direct detection of CB
  Direct detection of transition magnetic dipole moment of neutrino
  Direct measurement of neutrino mass:
Aiming at sensitivity of detecting from decay for
  SM expectation
  Current experimental lower limit
  L-R symmetric model (for Dirac neutrino) predicts down to for - mixing angle
LRS: SU(2)LｘSU(2)RｘU(1)B-L
SM: SU(2)Lｘ U(1)Y
Suppressed by , GIM
Only suppressed by
1026 enhancement to SM
Neutrino magnetic moment term
PRL 38,(1977)1252, PRD 17(1978)1395

## Slide 6: Photon Energy in Neutrino Decay
m3=50meV
m1=1meV
m2=8.7meV
E =4.4meV
E =24meV
Sharp Edge with 1.9K smearing
Red Shift effect
dN/dE(a.u.)
distribution in
meV]
E =24.8meV
Two body decay
()
()
()
From neutrino oscillation
From Planck+WP+highL+BAO
50meV<<87meV
  14~24meV (51~89m)

## Slide 7: Backgrounds to CB decay
at λ＝50μm
Zodiacal Emission
~8MJy/sr
CIB
~0.1-0.5MJy/sr
~0.5MJy/sr
s
~25kJy/sr
Expected spectrum
CMB
ZE
ZL
ISD
SL
DGL
CB decay
wavelength [m]
E [meV]
Surface brightness I [MJy/sr]
AKARI
COBE
CB decay

## Slide 8: Detector requirements
Need continuous spectrum of photon energy around 𝜆=50𝜇m (far infrared photon) with highly precise accuracy
  Photon-by-photon energy measurement with better than 2% resolution for (𝜆=50𝜇m ) to achieve better S/N as well as to identify the sharp edge in the spectrum
  A ground based experiment is impossible, so rocket and/or satellite experiment with this detector is required
Superconducting Tunneling Junction (STJ) detectors in development
  Array of 50 Nb/Al-STJ pixels with diffraction grating covering
    For rocket experiment aiming at improvement of current lower limit for by 2 order : O(1014yr) in a 200-sec measurement
  STJ using Hafnium: Hf-STJ for satellite experiment
    : Superconducting gap energy for Hafnium
    for 25meV photon: if Fano-factor is less than 0.3

## Slide 9: STJ(Superconducting Tunnel Junction）Detector
A bias voltage (|V|<2) is applied across the junction.
A photon absorbed in the superconductor breaks Cooper pairs and creates tunneling current of quasi-particles proportional to the photon energy.
Superconducting / Insulator /Superconducting Josephson junction device
Δ: Superconducting gap energy

## Slide 10: STJ examples
STJs are already in practical use as a single photon spectrometer for a photon ranging from near-infrared to X-ray, and shows excellent performances comparing to conventional semiconductor detectors
5mm
5mm
H. Sato (RIKEN)
100mm x 100mm
5.9KeV X-ray
But no example for far-infrared photon

## Slide 11
STJ energy resolution
Statistical fluctuation in number of quasi-particles determines STJ energy resolution
Smaller superconducting gap energy Δ yields better energy resolution
 | Si | Nb | Al | Hf
Tc[K] |  | 9.23 | 1.20 | 0.165
Δ[meV] | 1100 | 1.550 | 0.172 | 0.020
Δ: Superconducting gap energy
F: fano factor
E: Photon energy
Hf
Hf-STJ as a photon detector is not established
Nq.p.=25meV/1.7Δ=735
  2% energy resolution is achievable if Fano factor <0.3
Tc :SC critical temperature
Need ~1/10Tc for practical
operation
Nb
Well-established as Nb/Al-STJ
(back-tunneling gain from Al-layer)
Nq.p.=25meV/1.7Δ=9.5
Poor energy resolution, but photon counting is possible in principle
In both cases, developments are challenging
Notes: 11

## Slide 12
Proposal of a rocket experiment
  Expect 200s measurement at altitude of 200~300km
    Telescope with diameter of 15cm and focal length of 1m
    All optics (mirrors, filters, shutters and grating) will be cooled below 4K
  Diffraction grating covering =40-80m (16-31meV) and array of Nb/Al-STJ pixels: 50()x8()
  Use each Nb/Al-STJ pixel as a single-photon counting detector for FIR photon of ()
  sensitive area of 100mx100m for each pixel (100rad x 100rad)
Nb/Al-STJ array

## Slide 13: Expected accuracy in the spectrum measurement
Telescope parameters
Main mirror
  D=15cm, F=1m
detector
  sensitive area 100mx100m/ pixel
  50x8 array
CMB
ISD
SL
DGL
CB decay
wavelength [m]
Surface brightness I [MJy/sr]
Zodiacal Emission
Zodiacal Light
  Zodiacal emission 343Hz / pixel
  200sec measurement: 0.55M events / 8 pixels (at )
  0.13% accuracy measurement for each wavelength: =11kJy/sr
Neutrino decay (, yr): =25kJy/sr
  2.3σ away from statistical fluctuation in ZE measurement
Integrated flux from galaxy counts
 decay with yrs is possible to detect, or set lower limit!

## Slide 14: Summary
We propose an experiment to search for neutrino radiative decay in cosmic neutrino background.
Requirements for the detector is an ability of photon-by-photon energy measurement with better than 2% energy resolution for meV ()
Nb/Al-STJ array with grating and Hf-STJ are considered for the experiments and under development.
It is possible to improve the neutrino lifetime lower limit up to O(1014yrs) for 200-sec measurement in a rocket experiment with the detector.
Status of Nb/Al-STJ array development will be presented in T. Okudaira’s talk

## Slide 15: Backup

## Slide 16: Energy/Wavelength/Frequency

## Slide 17: STJ I-V curve
Sketch of a current-voltage (I-V) curve for STJ
The Cooper pair tunneling current (DC Josephson current) is seen at V = 0, and the quasi-particle tunneling current is seen for |V|>2
Josephson current is suppressed by magnetic field
Leak current
B field

## Slide 18: STJ back tunneling effect
Photon
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb/Al-STJ Nb(200nm)/Al(10nm)/AlOx/Al(10nm)/Nb(100nm)
Gain: 2～200
Nb
Al
Nb
Al

## Slide 19: Feasibility of VIS/NIR single photon detection
Assume typical time constant from STJ response to pulsed light is ~1μs
Assume leakage is 160nA
Fluctuation from electron statistics in 1μs is
While expected signal for 1eV are
(Assume back tunneling gain x10)
  More than 3sigma away from leakage fluctuation

## Slide 20: Feasibility of FIR single photon detection
Assume typical time constant from STJ response to pulsed light is ~1μs
Assume leak current is 0.1nA
Fluctuation due to electron statistics in 1μs is
While expected signal charge for 25meV are
(Assume back tunneling gain x10)
  More than 3sigma away from leakage fluctuation
Requirement for amplifier
    Noise<16e
    Gain: 1V/fC  V=16mV

## Slide 21: Temperature dependence of Nb/Al-STJ leak current
Temperature dependence of leak current
 10nA at T=0.9K
T=0.4K
Magnetic field on
Rref=
Leak current can be reduced by using small junction size. We are testing STJ of 4m2 junction size
2nA @0.5mV
Need T<0.9K for detector operation
 Use 3He sorption or ADR for the operation in rocket experiment
Junction size: 100x100um2
21
This Nb/Al-STJ is produced by S. Mima (Riken)
40um2 Nb/Al-STJ I-V curve
 2nA
Junction size: 40um2
Need Ileak<0.1nA for single photon counting with S/N>103

## Slide 22: 100x100m2 Nb/Al-STJ response to NIR multi-photons
10 laser pulses in 200ns
NIR laser through optical fiber
We observed a response to NIR photons
Response time ~1μs
Corresponding to 40 photon detection (estimated by statistical fluctuations in number of detected photons)
50μV/DIV
0.8μs/DIV
Observe voltage drop by 250μV
Response to NIR laser pulse（λ=1.31μm)
Signal pulse height distribution
Pedestal
Pulse height dispersion is consistent with ~40 photons
-Pulse height (a.u.)
STJ
I
V
1k
T=1.8K
(Depressuring LHe)
Signal
T. Okudaira

## Slide 23: 4m2 Nb/Al-STJ response to VIS light at single photon level
Best fit f(x;)
1photon
2photon
3photon
0photon
event
μ
x2
minimum at μ=0.93
ndf=85
pulse hight(AU)
Assuming a Poisson distribution convoluted with Gaussian which has same sigma as pedestal noise:
T. Okudaira
Currently, readout noise is dominated, but we are detecting VIS light at single photon level
T=1.8K
(Depressuring LHe)

## Slide 24: Development of SOI-STJ
SOI: Silicon-on-insulator
  CMOS in SOI is reported to work at 4.2K by T. Wada (JAXA), et al.
A development of SOI-STJ for our application with Y. Arai (KEK)
  STJ layer sputtered directly on SOI pre-amplifier
Started test with Nb/Al-STJ on SOI with p-MOS and n-MOS FET
SOI
STJ
Nb
metal pad
K. Kasahara
STJ lower layer has electrical contact with SOI circuit
STJ
Phys. 167, 602 (2012)
K. Kasahara’s talk for detail
Photon detectors session3 at 15:00 on 6th

## Slide 25: Hf-STJ development
We succeeded in observation of Josephson current by Hf-HfOx-Hf barrier layer in 2010 (S.H.Kim et. al, TIPP2011)
However, to use this as a detector, much improvement in leak current is required. ( is required to be at pA level or less)
B=10 Gauss
B=0 Gauss
HfOx：20Torr,1hour
anodic oxidation：45nm
Hf(350nm)
Hf(250nm)
Si wafer
A sample in 2012
200×200μm2
T=80~177mK
Ic=60μA
Ileak=50A@Vbias=10V
Rd=0.2Ω
K. Nagata

## Slide 26: Hf-STJ Response to DC-like VIS light
20μV/DIV
50μA/DIV
Laser ON
Laser OFF
Laser pulse: 465nm, 100kHz
10uA/100kHz=6.2×108e/pulse
We observed Hf-STJ response to visible light
K. Nagata
~10μA
V
I

## Slide 27: 4m2 Nb/Al-STJ response to DC-like VIS light
0.5mV/div
20nA/div
I
V
VIS laser pulse (465nm) 20MHz illuminated on 4m2 Nb/Al-STJ
~10nA
10nA/20MHz=0.5×10-15 C =3.1×103 e
0.45 photons/laser pulse is given in previous slide
Laser OFF
Laser ON
Gain from Back-tunneling effect
Gal=6.7

## Slide 28: Development of SOI-STJ
by K. Kasahara
2mV /DIV
1 mA /DIV
500uV /DIV
10 nA /DIV
2mV /DIV
50uA /DIV
2mV /DIV
1 mA /DIV
We formed Nb/Al-STJ on SOI
Josephson current observed
Leak current is 6nA @Vbias=0.5mV, T=700mK
B=0
B=150 gauss
n-MOS
p-MOS
n-MOS and p-MOS in SOI on which STJ is formed
Both n-MOS and p-MOS works at T=750~960mK
VGS[V]
0.7V
-0.7V
IDS[A]

## Slide 29
SOI上のNb/Al-STJの光応答信号
Pedestal
Signal
Iluminate 20 laser pulses (465nm, 50MHz) on 50x50um2 STJ which is formed on SOI
Estimated number of photons from output signal pulse height distribution assuming photon statistics
Nγ = ~ 206±112
500uV /DIV.
1uS /DIV.
Noise
Signal
M : Mean
σ : signal RMS
σp : pedestal RMS
Confirmed STJ formed on SOI responds to VIS laser pulses
STJ on SOI response to laser pulse