## Slide 1: Development of far-infrared single-photon spectrometers based on superconducting tunnel junction for search for the cosmic background neutrino decay
Sep 28-30, 2015 / Epochal Tsukuba
Yuji Takeuchi (Univ. of Tsukuba)
on behalf of Neutrino Decay Collaboration
S. H. Kim, K. Takemasa, K. Kiuchi, K. Nagata, K. Kasahara, K. Moriuchi, R. Senzaki, S. Murakami, S. Yagi (U. Tsukuba), S. Matsuura (Kwansei Gakuin U.), H. Ikeda, T. Wada, K. Nagase (JAXA/ISAS), H. Ishino, A. Kibayashi (Okayama U.), S. Mima (RIKEN), T. Yoshida, R. Hirose, Y. Kato, C. Asano, T. Nakamura (U. Fukui), Y. Kato (Kinki U.), Y. Arai, M. Hazumi, I. Kurachi (KEK), S. Shiki, M. Ukibe, G. Fujii, M. Ohkubo (AIST), E. Ramberg, J. H. Yoo, M. Kozlovsky, P. Rubinov, D. Sergatskov (FNAL), S. B. Kim (Seoul National U.) and S. Kawahito (Shizuoka U.)

## Slide 2: Contents
Introduction to neutrino decay search
  Proposed rocket experiment
  Prospects for the neutrino decay search
Candidates for far-infrared single-photon spectrometer
  Nb/Al-STJ with diffraction grating
  Hf-STJ
Summary

## Slide 3: Neutrino
Neutrino has 3 mass generations (1, 2, 3)
Neutrino flavor states (e, , ) are not mass eigenstates
Neutrino flavor oscillates during the flight, and squared mass differences (, ) have been measured, but their absolute masses are not measured yet!
Heavier neutrinos (2, 3) are not stable
  Neutrino can decay through the loop diagrams
  Neutrino mass can be determined from the decay
However, neutrino lifetime is expected to be very long (much longer than the age of universe)
We adopt Cosmic neutrino background (CB) as the neutrino source for neutrino decay search

## Slide 4: Cosmic neutrino background (CB)
CMB
CB (=neutrino decoupling)
The universe is filled with neutrinos.
However, they have not been detected yet!
Density (cm-3)
~1s after the big bang

## Slide 5: Motivation of -decay search in CB
Search for in cosmic neutrino background (CB)
  Search for anomalous magnetic moment of neutrino
  Direct detection of CB
  Determination of neutrino mass:
Aiming at a sensitivity to lifetime for
  Standard Model expectation:
  Experimental lower limit:
  L-R symmetric model (for Dirac neutrino) predicts down to for - mixing angle
LRS: SU(2)LｘSU(2)RｘU(1)B-L
SM: SU(2)Lｘ U(1)Y
Suppressed by and GIM
Only suppressed by L-R mixing ()
1026 enhancement to SM
Magnetic moment term
(need L-R coupling)
PRL 38,(1977)1252, PRD 17(1978)1395

## Slide 6: Photon Energy (Wavelength) in Neutrino Decay
m3=50meV
m1=1meV
m2=8.7meV
E =4.4meV
E =24meV
 distribution in
E =24.8meV
Two body decay
()
()
()
From neutrino oscillation
From Planck+WP+highL+BAO
50meV<<87meV
  14~24meV (51~89m)
dN/d(a.u.)
[m]
100
500
10
Red Shift effect
Sharp Edge with 1.9K smearing
in the 3 rest frame

## Slide 7: CB decay signal and Backgrounds
at λ＝50μm
Zodiacal Emission(ZE)
~ 8 MJy/sr
CIB
~ 0.1-0.5 MJy/sr
~ 0.8MJy/sr
~ 25kJy/sr
Expected spectrum
Surface brightness I [MJy/sr]
CB decay
λ＝50 μm
E=25 meV
Excluded by S.H.Kim et. al 2012
E [meV]
wavelength [m]
CB decay
AKARI
COBE
CMB
ZE
ZL
DGL
ISD
SL
CIB summary from Matsuura et al.(2011)

## Slide 8: Detector requirements for neutrino decay search
High-precision photon energy spectrum around 𝜆=50𝜇m
  Photon-by-photon spectroscopy in the far-infrared region with better than 2% resolution for (𝜆=50𝜇m )
    Lower dark noise in the detector
    Identify the sharp edge in the spectrum from the neutrino decay
  Rocket- and/or satellite-borne telescope with this detector.
    A ground-based experiment is impossible.
Superconducting Tunneling Junction (STJ) detectors
  Array of 50 Nb/Al-STJ pixels with diffraction grating covering
    For a rocket experiment aiming at O(1014 yrs) in a 200-sec measurement
    Improve the current experimental lower limit for by 2 orders
  STJ using Hafnium: Hf-STJ for a satellite experiment
    : Superconducting gap energy for Hafnium
    for 25meV photon: is achievable

## Slide 9: Superconducting Tunnel Junction (STJ) Detector
A bias voltage (|V|<2) is applied across the junction.
A photon absorbed in the superconductor breaks Cooper pairs and creates tunneling current of quasi-particles proportional to the deposited photon energy.
Superconductor / Insulator /Superconductor Josephson junction device
Δ: Superconducting gap energy
2
E
Ns(E)
Superconductor
Superconductor
Insulator
Insulator
Superconductor
100m
300nm
Much lower gap energy (Δ) than FIR photon  Can detect FIR photon
Fast response (~s)  Suitable for single-photon detection

## Slide 10
STJ energy resolution
Statistical fluctuation in number of quasi-particles  energy resolution
Smaller superconducting gap energy Δ yields better energy resolution
 | Si | Nb | Al | Hf
Tc[K] |  | 9.23 | 1.20 | 0.165
Δ[meV] | 1100 | 1.550 | 0.172 | 0.020
Δ: Superconducting gap energy
F: fano factor
E: Photon energy
Hf
Hf-STJ is not established as a practical photon detector yet
Nq.p.=25meV/1.7Δ=735
  2% energy resolution is achievable if Fano factor <0.3
  for a single-photon
Tc :SC critical temperature
Need ~1/10Tc for practical
operation
Nb
Well-established as Nb/Al-STJ
(back-tunneling gain from Al-layers)
Nq.p.=25meV/1.7Δ=9.5
Poor energy resolution, but a single-photon detection is possible
Developments are challenging, yet worthwhile
Notes: 10

## Slide 11
Proposed rocket experiment
with a diffraction grating and Nb/Al-STJ array combination
  200-sec measurement at altitude of 200~300km
    Telescope with diameter of 15cm and focal length of 1m
    All optics (mirrors, filters, shutters and grating) will be cooled at ~1.8K
  At the focal point, diffraction grating covering =40-80m (16-31meV) and array of Nb/Al-STJ pixels of 50(in wavelength distribution) x 8(in spatial distribution) are placed
  Each Nb/Al-STJ pixel is used as a single-photon counting detector for FIR photon in ()
  Sensitive area of 100mx100m for each pixel (100rad x 100rad in viewing angle)
Nb/Al-STJ array
8 rows
50 columns

## Slide 12: Expected precision in the spectrum measurement
Telescope parameters
Main mirror
  D=15cm, F=1m
detector
  sensitive area 100mx100m / pixel
  50 x 8 array
CMB
ISD
SL
DGL
CB decay
wavelength [m]
Surface brightness I [MJy/sr]
Zodiacal Emission
Zodiacal Light
  Zodiacal emission 343Hz / pixel
  200sec measurement: 0.55M events / 8 pixels (at )
  0.13% accuracy measurement for each wavelength: =11kJy/sr
Neutrino decay (, yrs): =25kJy/sr
  2.3σ away from statistical fluctuation in ZE measurement
Integrated flux from galaxy counts
 decay with yrs is possible to detect, or set lower limit!

## Slide 13: Sensitivity to neutrino decay
Parameters in the rocket experiment simulation
telescope dia.: 15cm
50-column (: 40m – 80 m)  8-row array
Viewing angle per single pixel: 100rad  100rad
Measurement time: 200 sec.
Photon detection efficiency: 100%
Can set lower limit on 3 lifetime at 4-6  1014 yrs if no neutrino decay observed
If 3 lifetime were 2  1014 yrs, the signal significance is at 5 level

## Slide 14: Status of Nb/Al-STJ photon detector development
Temperature(K)
0.3
0.4
0.5
0.6
0.7
Leakage
100pA
1nA
10nA
100nA
Requirements for Nb/Al-STJ
Single-photon detection for E=25meV (=50m)
Detection efficiency: ~1
Dark count rate < 30Hz  leak current < 0.1nA
Sensitive area: 100m  100m per pixel
50m  50m Nb/Al-STJ fabricated in CRAVITY at AIST
Ileak<1nA achieved at AIST
Will test STJs with a smaller junction size
0.1nA
2.9mm
M. Ukibe et al., Jpn. J. Appl. Phys. 51, 010115 (2012)
M. Ohkubo et al., IEEE Trans. Appl. Super, 24, 2400208 (2014)

## Slide 15: 100x100m2 Nb/Al-STJ response to 465nm multi-photons
Laser pulse trigger
A response from Nb/Al-STJs to NIR-VIS photons at single-photon level was observed with a charge-sensitive amplifier at the room temperature
Response time of STJ: O(1μs)
Due to the readout noise, a FIR single-photon detection is not achieved yet
Need ultra-low noise readout system for STJ signal
Considering a cryogenic pre-amplifier close to STJ
2V/DIV
40μs/DIV
100x100m2 Nb/Al-STJ fabricated at CRAVITY
Pulse height dispersion is consistent with 10-photon detection in STJ
465nm laser through optical fiber
STJ
10M
T~350m
(3He sorption)
Charge sensitive
pre-amp.
shaper amp.

## Slide 16: Development of SOI-STJ
SOI: Silicon-on-insulator
  CMOS in FD-SOI is reported to work at 4K by T. Wada (JAXA), et al.
A development of SOI-STJ for our application
  STJ layers are fabricated directly on a SOI pre-amplifier board and cooled down together with the STJ
Started test with Nb/Al-STJ on SOI with p-MOS and n-MOS FET
SOI
STJ
Nb
metal pad
STJ lower layer has electrical contact with SOI circuit through VIA
J Low Temp Phys 167, 602 (2012)
VIA
STJ
capacitor
FET
700 um
640 um
C
SOI-STJ2 circuit
D
S
G

## Slide 17: FD-SOI on which STJ is fabricated
Both nMOS and pMOS-FET in FD-SOI wafer on which a STJ is fabricated work fine at temperature down below 1K
Nb/Al-STJ fabricated at KEK on FD-SOI works fine
We are also developing SOI-STJ where STJ is fabricated at CRAVITY
B~150Gauss
2mV/DIV
1mA/DIV
I-V curve of a STJ fabricated at KEK on a FD-SOI wafer
nMOS-FET in FD-SOI wafer on which a STJ is fabricated at KEK
gate-source voltage (V)
drain-source current
0
0.2
0.4
0.6
0.8
-0.2
1pA
1nA
1A
1mA

## Slide 18: Pre-amplifier development
STJ readout circuit to apply a constant voltage on STJ as well as integrate the tunnel current from response to a photon.
A charge-sensitive pre-amplifier in SOI for STJ readout is under development using the SPICE simulation supported by VDEC*
For the circuit design, parameterization of MOSFET Id-Vg(Vd) for the SPICE simulation is in progress with KEK and JAXA.
STJ
-
+
V=-0.4mV
Output
* VLSI Design and Education Center(VDEC), the U. Tokyo in collaboration with Synopsys, Inc., Cadence Design Systems, Inc., and Mentor Graphics, Inc.

## Slide 19: Hf-STJ development
We succeeded in observation of Josephson current by Hf-HfOx-Hf layer in 2010
S.H.Kim et. al, TIPP2011
However, to use this as a detector, much improvement in leak current is required. ( is required to be at pA level or less)
B=10 Gauss
B=0 Gauss
HfOx：20Torr,1hour
anodic oxidation：45nm
Hf(350nm)
Hf(250nm)
Si wafer
A sample in 2012
200×200μm2
T=80~177mK
Ic=60μA
Ileak=50A@Vbias=10V
Rd=0.2Ω

## Slide 20: Hf-STJ Response to DC-like VIS light
20μV/DIV
50μA/DIV
Laser ON
Laser OFF
Laser pulse: 465nm, 100kHz
10uA/100kHz=6.2×108e/pulse
We observed an increase of tunnel current in Hf-STJ response to visible light
~10μA
V
I

## Slide 21: Summary
We propose an experiment to search for neutrino radiative decay in cosmic neutrino background.
Requirements for the detector is an ability of photon-by-photon spectroscopy with better than 2% energy resolution at =50m ( meV) with low dark count rate (<30Hz)
Nb/Al-STJ array with a diffractive grating and Hf-STJ are considered for the experiment.
  Nb/Al-STJ fabricated at CRAVITY meets our requirements.
  FD-SOI readout for STJ signal is under development.
  Hf-STJ development is in progress, yet need much improvement.
Improvement of the neutrino lifetime lower limit up to O(1014yrs) is feasible for 200-sec measurement in a rocket-borne experiment with the detector.

## Slide 22: Backup

## Slide 23: Energy/Wavelength/Frequency

## Slide 24: STJ I-V curve
Sketch of a current-voltage (I-V) curve for STJ
The Cooper pair tunneling current (DC Josephson current) is seen at V = 0, and the quasi-particle tunneling current is seen for |V|>2
Josephson current is suppressed by magnetic field
Leak current
B field

## Slide 25: STJ back-tunneling effect
Photon
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb/Al-STJ Nb(200nm)/Al(10nm)/AlOx/Al(10nm)/Nb(100nm)
Gain: 2～200
Nb
Al
Nb
Al