## Slide 1: Development of Superconducting Tunnel Junction Detectors as a far-infrared single photon detector for neutrino decay search
TIPP 2014 Conference
Jun. 2nd-6th, 2014 / Amsterdam, The Netherlands
Yuji Takeuchi (Univ. of Tsukuba)
for Neutrino Decay Collaboration
S.H.Kim , K.Kiuchi , K.Nagata , K.Kasahara , T.Okudaira, T.Ichimura, M.Kanamaru, K.Moriuchi, R.Senzaki(Univ. of Tsukuba), H.Ikeda, S.Matsuura, T.Wada(JAXA/ISAS), H.Ishino, A.Kibayashi (Okayama Univ), S.Mima (RIKEN), T.Yoshida, S.Komura, K.Orikasa, R.Hirose(Univ. of Fukui), Y.Kato(Kindai Univ.), Y.Arai, M.Hazumi(KEK), E.Ramberg, J.H.Yoo, M.Kozlovsky, P.Rubinov, D.Sergatskov(Fermilab) S.B.Kim(Seoul National Univ.)

## Slide 2: Contents
Introduction to neutrino decay search
STJ detector developments
  Rocket experiment with Nb/Al-STJ
  Hf-STJ development
Summary

## Slide 3: Motivation of -decay search in CB
Search for in cosmic neutrino background (CB)
  Direct detection of CB
  Direct detection of transition magnetic dipole moment of neutrino
  Direct measurement of neutrino mass:
Aiming at sensitivity of detecting from decay for
  SM expectation
  Current experimental lower limit
  L-R symmetric model (for Dirac neutrino) predicts down to for - mixing angle
LRS: SU(2)LｘSU(2)RｘU(1)B-L
SM: SU(2)Lｘ U(1)Y
Suppressed by , GIM
Suppressed only by
1026 enhancement to SM
Neutrino magnetic moment term
PRL 38,(1977)1252, PRD 17(1978)1395

## Slide 4: Photon Energy in Neutrino Decay
m3=50meV
m1=1meV
m2=8.7meV
E =4.4meV
E =24meV
Sharp Edge with 1.9K smearing
Red Shift effect
dN/dE(a.u.)
distribution in
meV]
From neutrino oscillation
From Planck+WP+highL+BAO
50meV<<87meV, 14~24meV
51~89m
E =24.8meV
Two body decay
()
()
()

## Slide 5: CIB and ZE Backgrounds to CB decay
AKARI
COBE
Zodiacal Light
Zodiacal Emission
Galaxy evolution model
Galactic dust emission
Integrated flux from galaxy counts
CMB
at (λ＝50μm)
Zodiacal Emission
~500nW/m2/sr
CIB (COBE)
~30nW/m2/s
-decay ()
~30nW/m2/s
-decay ()
~1.5pW/m2/s
-decay ()
~1.5nW/m2/s
Expected spectrum

## Slide 6: Detector requirements
Requirements for detector
  Continuous spectrum of photon energy around (, far infrared photon)
  Energy measurement for single photon with better than 2% resolution for to identify the sharp edge in the spectrum
  Rocket and/or satellite experiment with this detector
Superconducting Tunneling Junction (STJ) detectors in development
  Array of 50 Nb/Al-STJ pixels with diffraction grating covering
    For rocket experiment aiming at launching in two years after the detector R&D completion (in 2017 in earliest), expecting improvement of current lower limit for by 2 order : O(1014yr)
  STJ using Hafnium: Hf-STJ for satellite experiment (after 2020)
    : Superconducting gap energy for Hafnium
    for 25meV photon: if Fano-factor is less than 0.3

## Slide 7: STJ(Superconducting Tunnel Junction）Detector
A bias voltage V is applied across the junction.
A photon absorbed in the superconductor breaks Cooper pairs and creates tunneling current of quasi-particles proportional to the photon energy.
Superconducting / Insulator /Superconducting Josephson junction device

## Slide 8: STJ I-V curve
Sketch of a current-voltage (I-V) curve for STJ
The Cooper pair tunneling current (DC Josephson current) is seen at V = 0, and the quasi-particle tunneling current is seen for |V|>2
Josephson current is suppressed by magnetic field
Leak current
B field

## Slide 9
STJ energy resolution
Statistical fluctuation in number of quasi-particles determines STJ energy resolution
Smaller superconducting gap energy Δ yields better energy resolution
 | Si | Nb | Al | Hf
Tc[K] |  | 9.23 | 1.20 | 0.165
Δ[meV] | 1100 | 1.550 | 0.172 | 0.020
Δ: Superconducting gap energy
F: fano factor
E: Photon energy
Hf
Hf-STJ as a photon detector is not established
Nq.p.=25meV/1.7Δ=735
  2% energy resolution is achievable if Fano factor <0.3
Tc :SC critical temperature
Need ~1/10Tc for practical
operation
Nb
Well-established as Nb/Al-STJ
(back-tunneling gain from Al-layer)
Nq.p.=25meV/1.7Δ=9.5
Poor energy resolution, but photon counting is possible
Notes: 9

## Slide 10
FIR single photon spectroscopy
with diffraction grating + Nb/Al-STJ array
for JAXA rocket experiment
  Expect 200sec. measurement at altitude of 200~300km
    Telescope with diameter of 15cm and focal length of 1m
    All optics (mirrors, filters, shutters and grating) will be cooled below 4K
  Diffraction grating covering =40-80m (16-31meV) and array of Nb/Al-STJ pixels: 50()x8()
  Use each Nb/Al-STJ pixel as a single-photon counting detector for FIR photon of
  sensitive area of 100mx100m for each pixel (100rad x 100rad)
Nb/Al-STJ array

## Slide 11: Expected Photon rate per 1pixel
Telescope
  Zodiacal emission 343Hz / pixel
  200sec measurement: 0.55M events / 8 pixels (at )
  0.13% accuracy measurement for each wavelength
  =0.6nW/m2/sr
Neutrino decay (yr)
  =1.5nW/m2/sr
  2.3σ away from fluctuation in zodiacal emission measurement
Zodiacal Light
Zodiacal Emission
Galaxy evolution model
Galactic dust emission
Integrated flux from galaxy counts
CMB
yr
 with yr is possible to detect!

## Slide 12: Temperature dependence of Nb/Al-STJ leak current
Temperature dependence of leak current
 10nA at T=0.9K
T=0.4K
Magnetic field on
Rref=
Leak current can be reduced by using small junction size. We are testing STJ of 4m2 junction size
2nA @0.5mV
Need T<0.9K for detector operation
 Use 3He sorption or ADR for the operation in rocket experiment
Junction size: 100x100um2
12
This Nb/Al-STJ is produced by S. Mima (Riken)
40um2 Nb/Al-STJ I-V curve
 2nA
Junction size: 40um2
Need Ileak<0.1nA for single photon counting with S/N>103

## Slide 13: 100x100m2 Nb/Al-STJ response to NIR multi-photons
10 laser pulses in 200ns
NIR laser through optical fiber
We observed a response to NIR photons
Response time ~1μs
Corresponding to 40 photon detection (estimated by statistical fluctuations in number of detected photons)
50μV/DIV
0.8μs/DIV
Observe voltage drop by 250μV
Response to NIR laser pulse（λ=1.31μm)
Signal pulse height distribution
Pedestal
Pulse height dispersion is consistent with ~40 photons
-Pulse height (a.u.)
STJ
I
V
1k
T=1.8K
(Depressuring LHe)
Signal
T. Okudaira

## Slide 14: 4m2 Nb/Al-STJ response to VIS light at single photon level
Best fit f(x;)
1photon
2photon
3photon
0photon
event
μ
x2
minimum at μ=0.93
ndf=85
pulse hight(AU)
Assuming a Poisson distribution convoluted with Gaussian which has same sigma as pedestal noise:
T. Okudaira
Currently, readout noise is dominated, but we are detecting VIS light at single photon level
T=1.8K
(Depressuring LHe)

## Slide 15: Development of SOI-STJ
SOI: Silicon-on-insulator
  CMOS in SOI is reported to work at 4.2K by T. Wada (JAXA), et al.
A development of SOI-STJ for our application with Y. Arai (KEK)
  STJ layer sputtered directly on SOI pre-amplifier
Started test with Nb/Al-STJ on SOI with p-MOS and n-MOS FET
SOI
STJ
Nb
metal pad
K. Kasahara
STJ lower layer has electrical contact with SOI circuit
STJ
Phys. 167, 602 (2012)
K. Kasahara’s talk for detail
Photon detectors session3 at 15:00 on 6th

## Slide 16: Hf-STJ development
We succeeded in observation of Josephson current by Hf-HfOx-Hf barrier layer in 2010 (S.H.Kim et. al, TIPP2011)
However, to use this as a detector, much improvement in leak current is required. ( is required to be at pA level or less)
B=10 Gauss
B=0 Gauss
HfOx：20Torr,1hour
anodic oxidation：45nm
Hf(350nm)
Hf(250nm)
Si wafer
A sample in 2012
200×200μm2
T=80~177mK
Ic=60μA
Ileak=50A@Vbias=10V
Rd=0.2Ω
K. Nagata

## Slide 17: Hf-STJ Response to DC-like VIS light
20μV/DIV
50μA/DIV
Laser ON
Laser OFF
Laser pulse: 465nm, 100kHz
10uA/100kHz=6.2×108e/pulse
We observed Hf-STJ response to visible light
K. Nagata
~10μA
V
I

## Slide 18: Summary
We propose an experiment to search for neutrino radiative decay in cosmic neutrino background
We are developing a detector to measure single photon energy with <2% resolution for .
  Nb/Al-STJ array with grating and Hf-STJ are being considered
We observed Nb/Al-STJ response to VIS light at single photon level, but readout noise is currently dominated.
We’ve confirmed the SIS structure in our Hf-STJ prototypes and observed quasi-particle tunneling current from response to VIS light illumination
  but much improvement in leakage current is required for a practical usage
Development of readout electronics for Nb/Al-STJ is underway
  As the first milestone, aiming to single VIS/NIR photon counting
  Several ultra low temperature amplifier candidates are under development. SOI-STJ is one of promising candidates

## Slide 19: Backup

## Slide 20: Energy/Wavelength/Frequency

## Slide 21: Cosmic neutrino background (CB)
CMB
CB

## Slide 22: STJ back tunneling effect
Photon
Quasi-particles near the barrier can mediate Cooper pairs, resulting in true signal gain
  Bi-layer fabricated with superconductors of different gaps Nb>Al to enhance quasi-particle density near the barrier
  Nb/Al-STJ Nb(200nm)/Al(10nm)/AlOx/Al(10nm)/Nb(100nm)
Gain: 2～200
Nb
Al
Nb
Al

## Slide 23: Feasibility of VIS/NIR single photon detection
Assume typical time constant from STJ response to pulsed light is ~1μs
Assume leakage is 160nA
Fluctuation from electron statistics in 1μs is
While expected signal for 1eV are
(Assume back tunneling gain x10)
  More than 3sigma away from leakage fluctuation

## Slide 24: Feasibility of FIR single photon detection
Assume typical time constant from STJ response to pulsed light is ~1μs
Assume leak current is 0.1nA
Fluctuation due to electron statistics in 1μs is
While expected signal charge for 25meV are
(Assume back tunneling gain x10)
  More than 3sigma away from leakage fluctuation
Requirement for amplifier
    Noise<16e
    Gain: 1V/fC  V=16mV

## Slide 25: 4m2 Nb/Al-STJ response to DC-like VIS light
0.5mV/div
20nA/div
I
V
VIS laser pulse (465nm) 20MHz illuminated on 4m2 Nb/Al-STJ
~10nA
10nA/20MHz=0.5×10-15 C =3.1×103 e
0.45 photons/laser pulse is given in previous slide
Laser OFF
Laser ON
Gain from Back-tunneling effect
Gal=6.7

## Slide 26: Development of SOI-STJ
by K. Kasahara
2mV /DIV
1 mA /DIV
500uV /DIV
10 nA /DIV
2mV /DIV
50uA /DIV
2mV /DIV
1 mA /DIV
We formed Nb/Al-STJ on SOI
Josephson current observed
Leak current is 6nA @Vbias=0.5mV, T=700mK
B=0
B=150 gauss
n-MOS
p-MOS
n-MOS and p-MOS in SOI on which STJ is formed
Both n-MOS and p-MOS works at T=750~960mK
VGS[V]
0.7V
-0.7V
IDS[A]

## Slide 27
SOI上のNb/Al-STJの光応答信号
Pedestal
Signal
Iluminate 20 laser pulses (465nm, 50MHz) on 50x50um2 STJ which is formed on SOI
Estimated number of photons from output signal pulse height distribution assuming photon statistics
Nγ = ~ 206±112
500uV /DIV.
1uS /DIV.
Noise
Signal
M : Mean
σ : signal RMS
σp : pedestal RMS
Confirmed STJ formed on SOI responds to VIS laser pulses
STJ on SOI response to laser pulse