## Slide 1: Silicon Detectors
K. Hara
University of Tsukuba
Faculty of Pure and Applied Sciences
EDIT2013 March 12-22,2013

## Slide 2: Applications of Si detectors
vertexing
tracking
whole tracking
VLSI
UA2
F. Hartmann (2009)
First transistor invented 1947 (Shockley, Bardeen, Brattain)
Ge(Si ) diodes used for particle detection in 50s
HEP
follows a la Moore’s law

## Slide 3: NA11 (CERN)
• Aim: measure lifetime of charm
quarks (decay length ct~30 μm)
⇒ spatial resolution better 10μm required
24 x 36 mm2 size per chip
1200 strips, 20 μm pitch
240 read-out strips
250-500 μm thick bulk material
⇒ Resolution of 4.5 μm
D-K+p-p-
size:24x36mm
First operational Si strip detector used in experiment
First observation of Ds

## Slide 4: Vertexing at colliders
ev
qq->j2j4
B-hadron ->j3
->j1
B-hadron lifetime: ~2ps
decay length~ gbct=p/m*0.3[mm]
11cm

## Slide 5: CDF Silicon Tracker
Vertexing (L0+SVX2: 1SS+5DS)
Intermediate Silicon Layers (2 DS)
CDF extended Si coverage to tracking for the momentum measurement, outside the vertexing region.
Si detector required for high particle density
22cm
64cm

## Slide 6: ATLAS SCT
~2000 Barrel modules
~2000 EC modules
Robotic mounting

## Slide 7
Largest System: CMS
automated module assembly
endcap

## Slide 8: Lecture outline
Why silicon?
  Semiconductor
  Diode p-n junction
Planar Si detector
  Full depletion
  IV, CV
  Signal processing example
Radiation resistance
Relatives of planar microstrip sensors
Work on Si detector: Practical notice

## Slide 9: Advantages of Si Detectors
Industrial CMOS process adoptable
  micron order manufacturing is possible
  rapid development of technology (reduction of cost, but still high/area)
  (easy) integration with readout electronics for identical materials used
Low ionization energy & high density (solid)
  3.67eV/e-h compared to gas detectors (Xe/Ar:22/26 eV/e-ion), scintillator (100eV/g )
  thin device possible with small diffusion effect, resulting in sx<10mm achievable
  self-sustainable structure (compact detector)
High intrinsic radiation hardness
  applicable in HEP experiments and for X-ray image sensors
cons

## Slide 10: Why Silicon?
Silicon is 2nd most abundant element on Earth
Silicon semiconductor is realized by:
appropriate band gap (1.1eV)
excellent insulator SiO2 (~107 V/cm)
good neighbors B (as donor) and P (as acceptor)
group
In a pure silicon crystal,
Periodic Table
metal
non-metal
noble gas
/family
4 bonding electrons
n-type silicon
V in IV: electron excess
III in IV: electron deficit
p-type silicon
hole

## Slide 11: “appropriate” band-gap
band: when single atoms combine, outer quantum states merge, providing a large number of energy levels for electrons to take.
electrons in conduction band: free
electrons in valence band: tied to atoms
m: highest energy
level at T=0K
typical semiconductor ‘s band gap:
Si(1.1eV) Ge(0.67eV)
B.G.>9eV(SiO2)
B.G.～1eV
At room temperature, “small” number of free electrons in C.B. in semiconductor
probability of finding electron in state ei:
(Fermi-Dirac distri.)
or
(Maxwell-Boltzmann distr.)
semiconductor devices utilize them as signal carries
kT=0.026eV @RT
~10-10 (Dei:1.1eV)
no intensive cooling required
Interatomic distance

## Slide 12: Doped Semiconductor
:state density
states occupied
un-occupied
most of donors (electrons) => more electrons in C.B.
acceptors (holes) => more holes in V.B.@RT
more conductive than intrinsic
Notation i: intrinsic (does not appear in usual application)
n,p (n-,p-): lightly doped semiconductor (main sensor part)
n+,p+: heavily doped semiconductor (used as “electrode conductor”)
intrinsic : semi-conductive by thermal excitation
0.045eV
1.1eV
NA,ND: density of acceptor, donor atoms
n,p: density of electron, hole carriers

## Slide 13: Carrier concentration
In intrinsic silicon
F(E)
gC(E)
E
Resistivity:
330 kWcm @T=300K
@T=300K
In doped silicon
/cm3
Law of mass action : When p increased to Npi by doping, part of them recombine with ni such that n reduced to ni /N
: neutrality
NA: acceptor atoms are negatively charged
In n-type, n>>p , NA~0, ND>p
For (majority) n~ND~1012/cm3,
(minority) p~2x1020/1012=2x108/cm3
high r Si for typical n-bulk sensor
effective number of states in C.B.
carrier density
state density in CB
@T=300K

## Slide 14: Diode (pn-junction)
n-type
p-type
+
e-h recombine
(thermal diffusion)
no carrier region, but charged!
(depletion region)
“built-in potential” : Vbi
n+
p
Depletion region extends more in lightly doped side
n
p
+
-
Band level
~ 0.2V
(high r Si)
heavily doped
lightly
space charge density
e-carrier density
preventing further carriers to diffuse
E field
voltage
Ex
x

## Slide 15: Diode (pn-junction)
I=I0(eeV/kT-1)
-I0
with external bias
reverse bias: Vpn<0
Vpn-|Vbi|
-(|Vpn|+|Vbi|)
forward bias: Vpn>0
thermal diffusion only

## Slide 16: Planar microstrip silicon
n+
p-bulk
p+
Al
(implant)
(diffusion)
(evaporation)
Junction
(depletion develops)
p-p+: ohmic contact
low impedance connection between
Al electrode and p-bulk
300um
typ.
reverse
bias
d
Resistivity (of p-bulk)
Carrier mobility (480 vs 1350 cm2/Vs for p vs n-bulk)
-
+
[um]
Vb | 1 kWcm | 4 kWcm
n-bulk | 320V | 80V
p-bulk | 880V | 220V
full depletion voltage for 300um
ca.1014/cm2/(1um)
J. Kemmer (1980)

## Slide 17: Carrier mobility
hole
electron
drift velocity
E-field
For E=200V/300um, 100V/300um
depends on carrier density, temperature & E-field
Electrons: t(300um)=4ns, 6ns
Holes: t(300um)=12ns, 20ns
@RT and in high resistive bulk
cm2/s/V
Typical gas drift (v=5us/cm): t(2mm)~400ns

## Slide 18: High purity silicon
e.g. 4 kWcm resistivity
ND~3x1012/cm3
NA~1x1012/cm3
silicon crystal:
standard IC: a few Wcm
N ~5x1022 atoms/cm3
cf
M-Czochralski
Float-zone
crucible (Pt)
RF heater
(no contact)
single crystal
poly-silicon
~30cmf
magnetic field to dump oscillation in the melt
standard high resistivity silicon (15cmf) used to make HEP detectors
new for HEP detector:
high oxygen content helps improve rad-hardness & cheaper
~10kWcm
melting & crystallization purifies the silicon: ”segregation”
carriers contribute resistivity

## Slide 19: Microstrip
ATLAS SCT p+-on-n sensor: HPK
Edge implant
Guard ring
Bias ring
1mm(~3xthickness)
poly-crystalline
silicon
(~1MW/mm)
DC pad (testing)
AC pad (wire bond)
p+ implant (16um=0.2pitch)
DC contact
(shiny part is aluminum)
r/o
floating
0V
(~0V)
dummy
Vbias
80um

## Slide 20: Planar microstrip silicon
p-bulk
p+
Al
300um
typ.
reverse
bias
-
+
Bias ring
d
SiO2 insulator
(coupling cap.)
backplane & edge are at Vbias
Guard ring
Vguard settled to minimize E-field
edge+surface current
leakage current
e
e
e
e
e
h
h
h
h
h
1. e-h pair created /3.6eV
(1.1eV+lattice vibration) => 80eh/1um
2. Carriers drift to electrodes, inducing
charge on “nearby” electrodes
3. signal pulse picked up by amp.
Rbias
~1.5M
Cint~0.5pF/cm
Cback~0.2pF/cm
Ccp~20pF/cm
w/o depletion:
(#carriers=Nhx0.1x0.3x10mm)~109>>(signal)80x300
signal carriers recombine

## Slide 21: Further implants
P-bulk
- - - - - -
- - - - - -
- - - - - -
- - - -
p-stop ca.1013/cm2
Fixed positive charges at Si-SiO2 interface
attracts mobile electrons,
which shorts n+ electrodes together
SiO2
p-stop: p+ blocking electrode
P-bulk
- - - - - -
- - - - - -
- - - - - -
- - - -
p-spray ca.2x1012/cm2
SiO2
p-spray: uniform p+
(no mask, moderate density)
n-bulk
- - - - - -
- - - - - -
- - - - - -
- - - -
SiO2
n+-on-p
n+-on-n
p+-on-n
- - - - - -
p+-n-p+
(isolated)
HISTORICALLY
large Si detector systems employed:
n+-on-n in addition
p+-on-n
… simple
… double sided
n+-on-p
n+-on-n (single)
rad resistance
LHC

## Slide 22: Double sided microstrip
Want to readout from ends of ladder
90o strips routed by 2nd metal*
small stereo readout
CDF SVX2F
r/o chips
*ultimate strip technology
double-sided expensive process
r/o
r/o

## Slide 23: P-stop - some detail
“common” p-stop: p-stop lines connected together over the strip ends
“individual” or “atoll” p-stop: p-stop encloses each implant
Bias ring
Any flaw may affect to all strips
Need more space
Interstrip capacitance is an important parameter for S/N: small for both design

## Slide 24: Guard ring
Si breakdown E(30V/um)
Pre-irradiation
TCAD simulation on E, f
0V(BR)
-1kV(back)
VERTEX2011
GRs are floating.
f settled to minimize E

## Slide 25: IV – leakage current
Bulk current
n+
p+
depleted p
undepleted p
responsible for bulk current generation
d
characteristic Temp dependence
increase with radiation dose
constant beyond full depletion
2. Surface current
slow increase above full dep (non-constant component)
may substantial at low Vb
3. micro-discharge (quick increase at high bias)
carrier accelerated (mfp~30nm@RT) enough to create another e-h pair=> avalanche multiplication
occur at high E (design, scratch,,,)
I3 decreases with T (more disturbance for avalanche)

## Slide 26: Temperature dep. of leakage current
Diffusion current: negligible for a fully depleted devices
Generation current:
  - Thermal generation in the depleted region
Thermal runaway:
Reduced using long lifetime (t0) material (= pure and defect free)
Generation current is doubled for DT=7-8K
(approximately)
Opposite to metals where leakage decreases with temperature
Current
increase
Heat
device
Temperature
increase
Proper heat sink required in some applications

## Slide 27: CV – bulk capacitance
(Vb<VFD)
(Vb>VFD)
parallel plate condenser approx
Si permittivity
nF/mm
n+
p+
undepleted p
A: effective plate area
1/C2
VFD
Vb
Strip structure
Notes: p

## Slide 28: Cint – interstrip capacitance
Cint
VFD
Vb
Interstrip region depletion
Rbias
~1.5M
Cint~0.5pF/cm
Cback~0.2pF/cm
Ccp~20pF/cm
Largest contribution to “Detector capacitance”
Qnoise ~ CDET x Vnoise
more signal deficit if Cint is large (AC device)
Keep Cint smaller (restriction from geometry)
LCR meter measures Z
resistive
inductive
capacitive
input
Z=R-jC/w
Rbias
w
Cbulk
w
Rbias
Cint
good with small w
f~1 kHz
good with large w
f~1 MHz
To measure C, substantial C contribution in the circuit is preferred:
values are typical
Notes: p

## Slide 29: Signal size
1.7MeV/(g/cm2)
=>390eV/um in Si
82eh/um
54eh/um
mean
frequency
Etrans/interaction
d-ray
Edep/thickness
thick material:
good sampling about the mean
“conceptual” explanation of Landau tail
medium thick
good sampling in lower energy
fluctuation in
higher energy
thinner
good sampling shifts lower
energetic electrons
close collision
distant collision
excitations
mean energy loss

## Slide 30: Signal processing – preamp+shaper
CR-RC shaping (example)
Pulse peaking time
choose time constant:
shorter – better two pulse separation
longer – better noise performance (next pg)
FrontEnd amplifier stage:
preamp + shaper amp
Purpose of shaper:
set a window of frequency range appropriate for signal (S/N improved)
constant time profile
  Pulse height sampling for further processing
  (discrimination, ADC,,,)
  Fast baseline restoration
RF,CF
gain&BW

## Slide 31: Noise components
Detector
Noise contributions from:
Leakage current (I)
Detector capacitance (CD)
Parallel resistance (Rp)
Series resistance (Rs)
ENC: equivalent noise charge in number of electrons at amplifier input
small I, tp
a,b: amplifier design – ENC (CD) largest typically
peaking time
@T=300K
small tp, large RP (bias resistor)
small RS (aluminum line resistance), large tp
LEP: 500+15CD
LHC: 530+50CD
Signal peaking time tp is an important factor
cf: signal charge~24000(300um)
significant for irradiated sensors
important for fast peaking
be small such that S/N>ca.10

## Slide 32: Signal processing on detector
ATLAS
Binary readout (ON/OFF)
3 BC(beam crossing) info
noise
hit
25ns BC
Stores hit pattern & sends the patterns at the corresponding trigger BCid
=5.28us

## Slide 33: Need more – of course
Communication + power cables: low-mass cable on detector
Patched outside the detector volume to Communication : optical fiber cables
Power: bulky cables

## Slide 34: Radiation damage - mechanism
Point defects
MeV g,e, 10MeV p
MeV n
Cluster defects
disordered region
High energy particles: Point Defects+Cluster Defects
Hole trap
Holes created in insulator are less mobile, insulators are charged
Degrades strip isolation, induce surface current(?)
(Surface damage)
(Bulk damage)
Carrier trap, leakage current, change Neff (n->p)
Dose [Gy]
Fluence [1-MeV neutron-equivalent/cm2]

## Slide 35: NIEL – non-ionizing energy loss
Energy loss due to other than ionization
Difference due to
different energy
different particle type
D(E) scaled to 1-MeV equivalent damage:
1-MeV neq/cm2
1st level comparison
Fails in some cases
G.Lindstroem (2003)

## Slide 36: Impact of Defects on Detector properties
Shockley-Read-Hall statistics (standard theory)
Impact on detector properties can be calculated if all defect parameters are known: n,p : cross sections E : ionization energy Nt : concentration
Trapping (e and h)  CCE shallow defects do not contribute at room temperature due to fast detrapping
charged defects  Neff , Vdep e.g. donors in upper and acceptors in lower half of band gap
generation  leakage current Levels close to midgap most effective
enhanced generation  leakage current  space charge
Inter-center charge transfer model (inside clusters only)

## Slide 37: Defects identification
I. Pintille et al (2009)
Deep level transient spectroscopy
evaluate Ei from diode capacitance change with T
R.Wunstorf (1992)
Some identified defects
Most defects are acceptor like;
n-type sensor type-inverts after receiving certain radiation

## Slide 38: Temperature effect - annealing
P.Dervan et al
beneficial
reverse
ATLAS SCT
G.Lindstroem (2003)
Interstitials recombine with Vacancies
In longer term, vacancies combine with themselves or with impurity atoms to become stable defects
- time constant depends on temperature: ~ 500 years (-10°C) ~ 500 days ( 20°C) ~ 21 hours ( 60°C) - Consequence: Detectors must be cooled even when the experiment is not running!
V2, V3, VO, VC,,,

## Slide 39
Damage parameter  (slope in figure)
Leakage current (20degC, @VFD) per unit volume and particle fluence
 is constant over several orders of fluence and independent of impurity concentration in Si  can be used for fluence measurement
80 min 60C
Initial annealing completed, allowing comparison of irradiations in different conditions (irradiation rate)
Radiation damage - Leakage current

## Slide 40: Fluence at HL-LHC
I.Dawson: Vertex2012
1x1015
3x1014
5x1014

## Slide 41: Rad-hard: p-bulk sensor
P-bulk
n+-on-p
n-bulk
p+-on-n
p-bulk
Type inversion
Need full depletion for strip isolation
stays p (depletion develops always from strips)
operational at partial depletion if VFD exceeds the maximum allowed (reduced signal amount is tolerable by choosing the strip length shorter, thus smaller CD for noise)
radiation damage is less since faster electron carriers are collected (smaller trapping)
depletion
Fluence > a few 1014 /cm2

## Slide 42: Charge collection: p-bulk sensor for HL-LHC
un-irrad
S/N=10
S/N=10
Collectable charge decreases with fluence
Strip length is short (2.4cm) to cope with high particle density: this reduces CD hence noise
Vb~500V is enough to achieve S/N>10
short strips
(2.4cm long)
long strips
(9.6 cm long)

## Slide 43: Silicon Variations

## Slide 44: Silicon drift sensor
LHC-ALICE silicon drift sensor
Collect electrons towards the anode
(measure drift time to determine Y)
X
-Y
+Y
Spatial Resolution (ALICE testbeam)
20-40um in X (294um pitch)
30-50um in Y
depending on drift distance (diffusion)
-V
built-in resistors
Vdrift~8mm/us

## Slide 45: 3D silicon sensor
Charge loss after irradiation is primary due to carrier trap:
Shorten the carrier collection distance
PLANAR
\
50um
P+
n+
300um
P+
n+
n+
3D
Single-column (low E region)
Double-sided double-column

## Slide 46: PIXEL sensor
Powerful in track pattern recognition
(no ghost hits)
Pixel and readout interconnected by bumps (In or PbSn)
at LHC experiments
ATLAS: 50x400 um pixels (80M)
CMS: 100x150 um pixels (66M)
3 barrel layers+3/2 discs/EC
Notes: Lead-tin

## Slide 47: Monolithic device - SOI
On-pixel circuit
INTPIX4
512x832 pixels of (17um)2
Silicon-on-insulator

## Slide 48: Wire-bonding
pinches the wire controlling the tension
wedge to feed ultra-sonic power
Use ultra-sonic power to alloy the wire (20um diameter aluminum ) with target plate (aluminum)
wire be crushed to ca .twice the original thickness
no “viscus” (creation depends a lot on the surface)

## Slide 49: Handling cautions
Sensor surface is coated with thin layer of SiO2 or equivalent “passivation” (wire-bonding pads are not passivated): no super-clean required, though dusts may induce troubles
Ions trapped in insulator may degrade the insulator performance (vs HV). Na+ is typical ingredient of human : Do not touch by hand
MOS devices dislike electrostatic discharge: Ground yourself before handling
Large current may create permanent current path: Limit the current (1mA is too high)
Large current …: Cool high current sensors, required for irradiated sensors
Notes: sodium