5.Effect of charge up: Appendix

A diagnostic test of charge up effect is the measurements of both bias resistance and interstrip capacitance since the charge may short a number of strips and degrade their isolation. Four detectors have been tested before irradiation: sensor No.69 is easier to charge up compared to other sensors although the testing does not differ. The measurements performed on this sensor seem to reveal different surface effects: Fig.I and Fig.II show the results. Actually, it can be noted that the region at low bias resistance (D200) differs from the one with irregular interstrip capacitance (U100-U200).

Fig.I. Purdue results. BEFORE IRRADIATION Bias resistance versus strip number

Fig.II Purdue results. BEFORE IRRADIATION Interstrip capacitance versus strip number

The drop in the value of bias resistance can be explained by positive charge trapped in the silicon dioxide (see Tsukuba results). The observed patter of the interstrip capacitance is not related to any irregular behavior versus bias voltage.

After irradiation, the bias resistance measurements have been repeated and no irregular values are measured anymore (Fig.III). We may assume that the positive charge trapped in the silicon dioxide decays in time because:

-generated electrons tunnel through the potential barrier and recombine the vacancies (tunnel annealing);

-vacancies are emitted from traps  and move into the valence band (thermal annealing).

Fig.III Purdue results. AFTER IRRADIATION Bias resistance versus strip number

The interstrip capacitance measurements after irradiation are performed with three different set-ups: the sensor is either located on the chuck (both room temperature and T=12C) or inside the environmental chamber (T=-25C). Fig.IV shows that the interstrip capacitance has a value higher than the pre-irradiation value at voltage Vbias<400V; besides its behavior versus bias voltage does not follow the expected pattern. This effect is detected on sensor No.63 and No.69; it is not observed on sensor No.60.

The interstrip isolation decreases after irradiation due to interface state generation; nevertheless, we expect the interstrip capacitance to reach the pre-irradiation value at V(Vdep(130V.  The observed discrepancy might be explained assuming that oxigen vacancies (hole traps) are generated when the Si-Si bond breaks (mostly at the interface where the bonds are weak).

.

Fig.IV Purdue results. AFTER IRRADIATION Interstrip capacitance versus bias voltage

Since the defects inducing the irregular behavior of the capacitance don’t affect the bias resistance value, different impurities inside the silicon dioxide have to be assumed.

The capacitance measurements have been repeated one month later (the sensors are kept at temperature T=-7C except when testing). The results are shown in Fig.V.

Fig.V Purdue results. Interstrip capacitance versus bias voltage

The interstrip capacitance follows now our expectations: this reveals that the charge decays in time. Further studies are needed in order to better understand the behavior of impurities under radiation, nevertheless these tests prove the detectors to be radiation hard up to =1.4 *1014 1MeV eq-n.