## Slide 1
Sensors for the CDF Run IIb Silicon Detector
CDF Run IIb Silicon Group
L0~L5: r=2.1~16.6 cm
Sensor type | dimensions | strip pitch | number
Outer (axial) | mm2 | 37.5 m* | 1512
Outer (1.2o ) | mm2 | 40 m* | 648
L0 (axial) | mm2 | 25 m* | 144
*RO is double of these
Outer sensors (93% of all) are glued on both sides of
180 staves of 2 types (Axial-Axial or Axial-1.2o )
63 Outer (axial) and
53 Outer (1.2o ) sensors were fabricated by Hamamatu Photonics
114/116: No micro-discharge up to 1kV.
Other electrical/mechanical performance is also excellent.

## Slide 2
Five sensors were irradiated to 1.4x1014 n-eq/cm2
Full depletion voltage
Leakage current increase
as expected
Requires extra voltage to recover the performance:
0.7 X 1014 n/cm2
Interstrip Resistance (G
Interstrip capacitance :
(~300V for Vfd=130V)
Interstrip resistance:
(~1G at 300V)
Conclusions:
Prototype performance is satisfactory.
Production delivery starts from June.
Sensors for the CDF Run IIb Silicon Detector
Expected Dose (for 15 fb-1) at L0 for Run IIb is 0.7x1014 1 MeV n-eq/cm2.
Interstrip Capacitance (pF
1.4 X 1014 n/cm2