## Slide 1: Status of Hamamatsu Silicon Sensors
SCT@CERN, Oct 2001
Prepared by K. Hara (U. Tsukuba)

## Slide 2: Summary of Institution(+HPK) tests

## Slide 3: Delivery
200~300/month in recent deliveries
Production sensors with modified mask from March
2063

## Slide 4: Leakage current (@150, 350V)

## Slide 5: defects

## Slide 6: wafer thickness
full depletion voltage
recent
delivery

## Slide 7: Bias resistance, sampling 2/lot

## Slide 8: Implant tests: sampling (2/lot)
June 2001

## Slide 9: Full strip tests: just started…
Measure only detectors with many defects …
All defects identified
These not identified

## Slide 10
No new defects created!
visually not seen as well
Many HPK defects clustered 300-400: problem in HPK prober?
some (?) not identified:

## Slide 11
24hr I stability
1093 delivery
2063 delivery
Recent delivery