## Slide 1: Status of Hamamatsu Silicon Sensors
K. Hara (Univ of Tsukuba)
Delivery
leakage current at 150V & 350V
number of defect channels
wafer thickness & full depletion voltage
bias resistance (sampling)
Status of Institute tests
implant tests
Coupling capacitors
24-hr leakage current stability
SCT@Prague, June 2001

## Slide 2: Summary of Institution tests (status)

## Slide 3: Delivery
~100/month so far
Production sensors with modified mask from March
We aim at ~300/month.
1093

## Slide 4: Leakage current (@150, 350V)

## Slide 5: defects
all defects
pinhole is responsible…

## Slide 6: wafer thickness
full depletion voltage 50~90V
mean=289um
spec:285±15
recent
delivery

## Slide 7
November 2000
December 2000
HPK I-V curves

## Slide 8: IV curves
Detectors with new mask

## Slide 9: Bias resistance, sampling 2/lot

## Slide 10: Implant tests: sampling (2/lot)

## Slide 11: Coupling capacitors
Measure nly detectors with many defects …

## Slide 13: 24hr I stability

## Slide 14: Semi-auto prober